Note

Undecided

Check Ref.

Check logic

Design and Simulation of Sb2Se3-based Resonant Optical Limiters using Transfer Matrix Method

Surawut Wicharn1, Chettanat Padungatthakij2, Suebtarkul Suchat3, Nathan Hagen4, and Prathan Buranasiri2*

1 Department of Physics, Faculty of Science, Srinakharinwirot University, Bangkok, Thailand.

2 Department of Physics, School of Science, King Mongkut’s Institute of Technology Ladkrabang, Bangkok, Thailand.

3 Department of Physics, Faculty of Science and Technology, Phranakhon Rajabhat University, Bangkok, Thailand.

4 Department of Optical Engineering, Utsunomiya University, Tochigi, Japan.

* prathan.bu@kmitl.ac.th

# Abstract:

We proposed an optical limiter designs which utilize antimony triselenide (Sb2Se3). Optical limiter is a type of device that allows light transmission in one mode, but can be switched to block transmission. Sb2Se3 is a phase change material which has low loss in the IR spectrum, high and stable refractive index contrast in both visible and IR spectra, and a high phase switching endurance up to an order of 106 cycles. We compared the performances of single-layer, two-layer, three-layer, edge-filter, and Fabry-Perot designs for 532 and 1064-nm usage, both wavelengths required a different design approaches. At 1064 nm Sb2Se3 has no absorption so it is suitable as high efficiency optical limiters. But at 532 nm, Sb2Se3 exhibits high absorption which could be used as a self-activated phase-switching mechanism. Aside from optical performances, we also investigate their optical endurance using computer simulations. (134 words)

Keywords: optical limiter, resonant cavity, antimony triselenide, phase change material  (keywords  < 7)

# 1. Introduction

Phase change material (PCM) can have different meanings depending on the field. In energy storage, the term would refer to material that store and release thermal energy through changes in its state of matter (latent heat), and the transition occurs between solid and liquid state [1]. However, in electronics and photonics, the term PCM refers to a solid-state material that changes its crystal structure when its temperature rise above transition temperature (Ttrans). This change in crystalline structure leads to a change in its optical properties, i.e. complex refractive index [2]. Complex refractive index comprises of real refractive index (n) and imaginary extinction coefficient (k) parts, and the refractive index contrast between the two phases of PCM is an order of magnitude larger than contrast induced by applied electric field or light intensity (Kerr effect) [3, 4]. This property makes PCM ideal for photonic applications that require the modulation of light transmittance, absorptance, or reflectance. Examples include optical limiters[4-10], optical switches[11-14], optical filters[15-17], optical diode[18], and absorbers[19-21].

Phase change material can be classified by its behavior after phase transition occurs. A volatile PCM will revert to its pre-transitioned phase if temperature falls below Ttrans. But non-volatile PCM will remain in its transitioned phase even if temperature falls below Ttrans. To turn non-volatile PCM back to pre-transitioned phase it needs to be heated above melting temperature and then rapidly quenched. Popular examples of non-volatile PCMs are Ge2Sb2Te5 (GST) and Ge-Sb-Se-Te  (GSST). One of the earliest and most commonly studied non-volatile PCM is GST [22, 23]. It is a chalcogenide glass that has large refractive index contrast (Δn) between amorphous and crystalline phases. GST has low Ttrans at ~145 °C for cubical phase crystallization when compared to other non-volatile PCM, and it changes into hexagonal phase at ~200 °C [4, 24]. Its drawback is the large extinction coefficient (k) in both visible and IR spectra which causes high optical loss from absorption. Another popular non-volatile PCM is GSST (Ge2Sb2SexTex), it is a derivative of GST that substitutes some part of tellurium with selenium. It has a large refractive index contrast in the visible spectrum like GST but has a lower extinction coefficient which helps increase optical efficiency. But GSST has higher Ttrans at ~242 °C [24]. In the past 10 years, VO2 gathered attention as a volatile PCM with Ttrans close to room temperature. It undergoes a metal-insulator transition (MIT) at Ttrans of 68 °C and has relatively high refractive index contrast starting from near-IR (NIR) to IR with a small extinction coefficient in the insulating phase (cold state). Its main drawbacks are its large extinction coefficient in the metallic phase [23] and a noticeable thermal hysteresis [25]. Attempts have been made to decrease Ttrans of VO2 closer to room temperature, but these also reduce the switching endurance and refractive index contrast [26]. Beyond the above-mentioned applications, an example of VO2 usage is as thermochromic window coatings that helps with temperature regulation inside a room by blocking infrared sunlight in the summer, but allows light to come in during winter which helps with indoor heating [27-29].

Compared to other PCMs, antimony triselenide (Sb2Se3) is a relatively new material in the field of photonics, only one review paper existed prior to 2026 [30]. (recheck claims whether it’s still true). The initial research on Sb2Se3 is in solar-energy applications [31], but Sb2Se3 has recently gathered interest as a non-volatile PCM for photonic applications [30] because of its near-zero extinction coefficient in the IR spectrum, its extinction coefficients are also lower than GST in the visible spectrum for both amorphous and crystalline phases, it has a relatively high and stable refractive index contrast from visible to infrared, and the crystallization temperature of is between GST and GSST at ~186 °C [32]. Sb2Se3 has a fast switching time in a microsecond range [22, 32, 33]. Its phase-switching endurance is also high, with experimental demonstration showing that it can reach as high as 106 to 107 cycles with an optimized laser-induced crystallization and re-amorphization schemes [32, 33]. These properties make Sb2Se3 attractive for a low-loss, reconfigurable optical switches and circuits that are used in optical waveguide [11, 22, 34, 35]. Even so, to the best of our knowledge, Sb2Se3 applications as optical limiters have yet been explored.

Optical limiter is a photonic device that protects sensitive detector or eyes from high intensity light, it allows light to propagated through during its “ON” mode but will reflect or absorb light when switched to “OFF” mode. The device could be self-switching, i.e. undergoes a phase transition through light absorption [7, 8],  or it could switched by external means, such as joule heating [16], or laser-induced heating outside of its intended operating bandwidth [32]. The device could either be designed to operate over a broad wavelength [4-6, 36] or as single wavelength [7, 8, 37, 38]. An ideal optical limiter with highest efficiency maximizes transmittance in the ON mode and minimizes it in the OFF mode, while also minimizing reflectance and absorptance in both modes, but if it’s self-activating type, it should have just enough absorption to induce phase transition. Optical limiter designs could be a planar thin-film structures or a nanostructured metasurfaces; planar structures are easier to design, optimize and fabricate, but metasurface structures offer more design flexibility [8]. For a planar designs, there are many methods to create high transmission such as: 1) single or multi-layers antireflection (AR) designs and 2) Line-pass, long-pass, or short-pass filters [39]. All of these designs rely on resonance to achieve antireflection properties, but if the materials have high extinction coefficients (k), e.g. metals or some of the PCMs, the resonant condition will be disrupted. Resonance can be restore by the use of asymmetrical resonant cavity [40], this design incorporates high k-index material placed between two mirror-like layers. The cavity designs also reducing the total thickness of PCM when compared to other designs, this is especially helpful in the case of volatile PCMs because it reduces the total energy required to induce phase transitions. Another benefit of using thinner PCM is the reduction of stress damage from the contraction and expansion in crystallization and re-amorphization processes [17]. It also reduce partial phase transition which happened when film size is above its thickness limit and open up more laser optimization schemes for inducing phase transitions [32].

In this work, we investigate Sb2Se3-based optical limiters with a planar thin-film designs. The intended operating wavelengths are selected to be 1064 or 532 nm because they are from Nd:YAG laser and its second harmonic which are commonly used in laboratory setups. Another reason is that these two wavelengths have a different design approaches. In 1064-nm designs, Sb2Se3 has near-zero absorption in both phases and its refractive index contrast is stable throughout IR spectrum. The goal of the 1064-nm designs is to create a broadband (IR) optical limiter that have high transmission in the ON mode and reflected most of the light in the OFF mode. As for 532-nm designs, at this wavelength the extinction coefficients of Sb2Se3 are large for both amorphous and crystalline phases [22], which can be used for self-activating design. A simple antireflection, or a long/short-pass designs cannot achieve perfect antireflection conditions because of the absorption. Therefore, an asymmetrical resonant cavity design approach is used for 532-nm designs.

# 2. Theories

## 2.1 Optical Properties of Sb2Se3

The complex refractive index (ñ) of phase change material at any wavelength (λ) can be written as:

npλ=npλ+ikpλ						(1)

where the real term n is the refractive index, the imaginary term k is extinction coefficient, and p denotes the phase which for Sb2Se3 can either be amorphous (amo) or crystalline (cry). Dispersive models, such as Tauc-Lorentz or multi-oscillator fits are often used to represent the measured np and kp over the spectral range of interest. (need this part?). In this work, a linear interpolation is used since all the materials dataset used have the measurement interval of less than 4 nm. The complex refractive indices of Sb2Se3 at 532 nm are: ña = 3.962 + 1.093i, and ñc = 4.788 + 2.241i. And ñ at 1064 nm are: ña = 3.370 + 0.000i, and ñc = 4.308 + 0.010i. Figure 1 shows their ñ from 300 to 1700 nm using data from [22]. The blue line represents real refractive index (n), and the red line represents imaginary extinction coefficient (k). In amorphous phase (Fig. 1a), the refractive index increases from around 2.4 at 300 nm to a peak of around 4.0 at 600 nm and gradually decreases to a stable value of around 3.3 above 1200 nm, indicating a strong dispersion near the band edge of visible spectrum and a weaker dispersion in the NIR spectrum. The extinction coefficient starts at approximately 2.1 at 300 nm and dropped to zero at around 850 nm. In the crystalline phase (Fig. 1b), the refractive index is around the same value as that of amorphous phase but reached a peak of around 5.1 at around 660 nm, it is then dropped to a stable of 4.1 in the NIR spectrum. The k-index of crystalline phase peaked at around 3.1 in the near-UV spectrum and rapidly approach zero above 900 nm. So, antimony triselenide (Sb2Se3) refractive index contrast Δn = nc - na is large and stable in the visible through IR spectra, and extinction coefficients is very large in the near-UV but falls to zero around NIR spectrum for both phases, with crystalline phase exhibits higher absorption in the visible spectrum.

Fig. 1. Complex refractive index of Sb2Se3 in (a) amorphous, and (b) crystalline phases. The data are taken directly from [22].

## 2.2 Single-layer antireflection design

In designing optical limiters, we can first consider its optical performance in the ON mode first, and then consider its transmission contrast when switched to OFF mode. Most optical devices will either be optimized for antireflection (AR) or high reflection properties. But in this work, optical limiters are designed to utilize transmission and absorption only, minimizing reflection is beneficial (absorption is utilizes in phase transition).  The simplest thin-film device consists of a single film layer with no absorption deposit on a substrate. A single thin-film layer reflects light at two interfaces as shown in Fig. 2: the bottommost interface is between thin film and substrate (R1), and the topmost interface is air-film (R2). Antireflection condition occurs when destructive interference of R1 and R2 with the same amplitude and a phase difference of π radian (i.e. optical path length of λ/2) occurs. And since R1 travels through the film layer twice (transmitted down and reflected up), the film optical thickness only needs to be half of that, an optical thickness of λ/4 which also known as quarter-wave optical thickness (QWOT). Optical thickness (OT) is defined as the optical path length of wavelength (λ) through the film layer:

OT(λ)=n(λ)t,						(2)

where n is the refractive index of the film at λ, and t is the physical thickness of the film. For a single-layer AR device, the thin-film physical thickness (t) needs to be equal to:

t=OTn=λ4n.						(3)

Fig. 2. Light paths in a single-layer thin film device. R1 is the reflected light at the film-substrate interface, and R2 is the reflected light at the air-film interface. Antireflection occurs when the phase difference between the two is π radian. The reflection angles are exaggerated for illustration purpose; both angles are the same as incidents.

Another way to calculate the thickness required for AR condition is to consider the reflection of the device.  For a lone substrate with air as the initial incident medium, the reflectance (R) is related to Fresnel reflection coefficient (r) as the following:

R= r2=na-nsna+ns2,					(4)

where na is air refractive index, and ns is substrate refractive index. For single-layer film on a substrate, the combined film and substrate index is effective reflectance index (nr) [39]. It is defined as:

nr=nfns+nf+ns-nfe-i2θns+nf-ns-nfe-i2θ, 					(5)

where nf is the film refractive index, i denotes imaginary unit, and θ is the phase thickness which is related to optical thickness (OT) of the film by

θ=k0OT,						(6)

where k0 is the angular wavenumber (k0=2π/λ). By replacing ns with nr in Eq. 4, reflectance of a single-layer device become:

R=r2=na-nrna+nr2.					(7)

Antireflection condition is achieved when R = 0 or na = nr. This condition occurs when the phase thickness (θ) in Eq.5 is in multiple of π/2 radian, such as QWOT:

θ=Zπ2,							(8)

where Z can be any even integer. We can simplify Eq.5 using Euler’s identity (exp-iπ = -1) to:

nr=nfns+nf-ns-nfns+nf+ns-nf=nf2ns,					(9)

so, an antireflection condition happen when nr = na or:

nans=nf2.						(10)

Another condition to consider is that the relative refractive index between air, film, and substrate must be such that nair < nf < nsubstrate. Reflected light shift its phase by π radian when reflected from lower to a higher refractive index medium. The reflected light (R2) at air-film interface undergoes π radian phase shift since nair is the lowest in most cases, so R1 must also has it phase shifted by the same amount. These two conditions place a limitation on material refractive index selection, since for a complete antireflection, there exist only one ideal answer for each substrate. Since the QWOT design must have film refractive index higher than air  but lower than substrate, which in this work is silica (SiO2), but Sb2Se3 has refractive index greater than silica at both 532 and 1064 nm wavelengths, the R1 light travelled 2QWOT = π radian further than R2 but only R2 has its phase shifted by π radian after reflection at the air-film layer, so a constructive interference occurs instead. To create destructive interference, the film needs to be λ/2 or half-wave optical thick (HWOT) instead such that R1 would travel an extra 2HWOT = 2π radian further than R2. As an example, at the reference wavelength λ0 = 1064 nm, if we use 3-mm-thick SiO2 substrate with a refractive index of ns = 1.46 [41] the ideal film thickness needs to be QWOT and has a refractive index of 1.21 for a complete antireflection design. The value 1.21 is lower than any commonly available material and the material with the closest refractive index is MgF2 at 1.38 [42], this difference cause the reflection to be higher than an ideal film as can be seen in Fig. 3. In the case of Sb2Se3 (solid line), its thickness is instead HWOT. An ideal film still exhibits some reflection because we modelled the reflection from the back substrate-air interface.

Fig. 3. Reflectance comparison of each single-layer thin film design. At 1064 nm, Sb2Se3 (blue) has reflectance = 6.5%, MgF2 with nMgF = 1.38 (green) has reflectance = 5.0%, and an ideal film with nf = 1.21 (grey) has reflectance = 3.4%. The thickness of Sb2Se3 is HWOT, both ideal film and MgF2 are QWOT. The black vertical line indicates the targeted optical limiters operating wavelength λ = 1064 nm.

## 2.3 Multilayer antireflection design

A two-layer device with QWOT in each layer (Q/Q design) can also achieve a complete antireflection condition. The Fresnel reflection coefficient (r) from Eq. 7 can be expanded to:

r=na-nr2na+nr2,						(11)

r=na-(nf22nr1)na+(nf22nr1),	 					(12)

r=na-(nf22nf12/ns)na+(nf22nf12/ns),	 					(13)

where the film numbering (nf) starts from substrate side and increases toward air (ns / nf1 / nf2 / na), where nr2 is the effective reflectance index of the entire structure [39], and nr1 is the effective reflectance index of only substrate and bottom film. Antireflection condition (r = 0) occurs when:

na=nf22nf12/ns,						(14)

or:

nans=nf22nf12.						(15)

This means that the refractive index of the top film must be smaller than the bottom film (nf2 < nf1). As an example, at 1064 nm if we use the same SiO2 as substrate and Sb2Se3 as bottom film (nf1=3.37), the required refractive index of nf2 can be calculated to 2.78. A commonly used material with the closest refractive index is TiO2 with nf2=2.31 [43]. When compared to a single-layer Sb2Se3 design, two-layer design allows for wider materials selection, has lower reflectivity, and broader operation wavelength, as shown in Fig. 4. Another way to create a perfect AR condition is to fix the two materials refractive index and vary each layer thickness instead, as described in chapter 5.2 of [39]. However, this method narrows the antireflection bandwidth.

A three-layer design (Q/H/Q) has a HWOT layer placed in the middle. The required refractive index ordering of each layer is ns < nf1 < nf2 and nf2 > nf3 > na. The middle layer (nf2) acts an absentee layer when incident wavelength (λ) is the same as reference wavelength (λ0), but it acts as compensating layer to restore resonance for a scenario where λ differs from λ0, a more detailed explanation is provided in chapter 5.4 of [39]. The reflectivity from Eq. 7 is equal to:

r=na-nr3na+nr3=na-(nf32nr2)na+(nf32nr2).						(16)

Because the middle film layer (nf2) is HWOT thick, it behaves as an absentee layer [39, 44]. So nr2 = nr1 and Eq. 16 becomes:

r=na-(nf32nr1)na+(nf32nr1)=na-(nf32nf12/ns)na+(nf32nf12/ns).						(17)

A three-layer antireflection condition occurs when:

nans=nf32nf12.						(18)

The refractive index ratio between top and bottom film is the same ratio as the two-layer design. As an example, the bottom layer (nf1) is Sb2Se3 (QWOT), using Eq. 18, the top layer (nf3) refractive index is calculated to 2.78, so TiO2 (nf3 = 2.31) is used again. The middle layer needs to have the highest refractive index, so Silicon with nSi = nf2 = 3.55 [45] is used. This three-layer design reflectance at wavelength farther from λ0, such as at 1400 nm and above, is lower than that of a single or two-layer design which means the benefit of adding Si as middle layer is its contribution to a broader operational bandwidth [44].

But instead of placing Sb2Se3 as the bottom film layer, Sb2Se3 can be moved to the middle layer instead so that the selection of nf1 and nf3 becomes more practicable. The bottom layer could be Si3N4 (nf1 = 2.00) [46] so that the ideal top layer calculated from Eq. 18 have nf3 = 1.65, which Al2O3 has the closest refractive index at 1.62 [43]. These design are shown in Fig. 4 where the reflectance of the single-layer, two-layer, and three-layer designs, which have Sb2Se3 placed directly on top of the substrate (nf1 = Sb2Se3), are 6.5% to 6.7%. But the last design with Sb2Se3 placed in the middle (nf2 = Sb2Se3) has reflectance equal to 3.4%, the same value as an ideal single-layer design (3.4%) in Fig. 2. This improvement can be explained by the selection of both nf1 and nf3 that are closer to ideal values.

Fig. 4. Reflectance comparison of a single-layer, and multi-layer Sb2Se3 antireflection designs. The single-layer, two-layer and three-layer designs with Sb2Se3 as bottom layer (nf1) have around the same reflectance at 1064 nm of 6.5 - 6.7%. The three-layer design with Sb2Se3 as the middle layer (nf2) has the lowest reflectance at 3.4%. The black vertical line is λ = 1064 nm.

## 2.4 Long-pass edge-filter design

In all previous designs, the performance after phase transition has not yet been considered. Aside from low reflectance,  another requirement for optical limiter is a high reflectance contrast when the device changes its mode. Figure 5 shows the reflectance comparison between Sb2Se3 in amorphous (solid) and crystalline (dotted) phases, which represent optical limiter in the ON and OFF mode, respectively. The optical limiters designs are the same as described in Fig. 4. A single-layer design has the highest reflectance contrast of 55.0% (Fig. 5a). For the three-layer design with Sb2Se3 as the middle layer, even though it shows the lowest reflectance in amorphous phase at 3.4%, its reflectance in crystalline phase only increased to 14.8%, which make the reflectance contrast only at 11.4% (Fig. 5b).

Fig. 5. Reflectance comparison of optical limiter designs before (ON mode, solid) and after (OFF mode, dotted) the devices switch their mode. (a) Single-layer (blue) and two-layer designs (green). (b) Three-layer designs with Sb2Se3 on the bottom (orange) and in the middle layer (red). Single-layer design has the highest reflectance contrast. The vertical black lines indicate λ0 = 1064 nm.

Edge-filter design is a design that has high reflectance around reference wavelength (λ0) but exhibits strong antireflection property outside this region. We could design optical limiter such that the edge is near the operating wavelength, such that the reflectance profile will be shifted by the increase in refractive index of H layer after Sb2Se3 undergoes phase transition (or by lowering the refractive index of L layer in other PCM). Edge-filter design could have a stable antireflection property in wavelengths that are either longer or shorter than λ0 depending on the structure of unit cell; (H2LH2) for long-pass and (L2HL2) for short-pass design. Where H and L denote QWOT-thick materials with high and low refractive index, respectively, and 12 denotes a layer with QWOT2 thickness. Since edge-filter design exhibits high reflectance around λ0, and we want our optical limiters to operate at λ = 1064 nm, λ0 must be shifted from 1064 nm to either a shorter or longer wavelength. A shorter λ0 is preferred since it reduces the physical thickness in each layer (Eq. 3), so a long-pass (H2LH2) design will be used to create a stable AR condition. The spectral width of the high reflection region is determined by the refractive index difference between H and L layers, the larger the refractive index contrast, the broader the spectral width. The steepness of the spectral edge is directly correlated to the numbers of unit cells, with higher numbers of unit cells correspond to steeper edge. Figure 6 shows long-pass (H2LH2) unit-cell designs; with Sb2Se3 as H and MgF2 as L layer, N indicates the number of unit cell used, and reference wavelengths (λ0) are set to 750 nm. Figure 6a is the reflectance comparison between different numbers of unit cells, designs with higher numbers of unit cell have a sharper spectral edge. It is interesting to note that the 8-unit-cell design (dotted) has a sharper edge than the 4-unit-cell design (loosely dashed), but the reflectance of 8-unit-cell design at around 1350 and 1650 nm are higher, so a higher numbers of unit cells does not necessarily give better performance. Figure 6b shows a comparison between amorphous and crystalline phases of 4 unit-cell Sb2Se3 design; the reflectance in amorphous and crystalline phase are 6.5% and 94.1%, respectively. So, the reflectance contrast at 1064 nm is 87.6% which is the highest among any designs shown. Another point to note is that the reflectance in amorphous phase is around the same value as other optical limiter designs with Sb2Se3 layer directly deposited on top of the SiO2 substrate.

Fig. 6. Reflectance comparison of long-pass designs (H2LH2) with (a) varying number of unit cells. (b) Design with 4-unit cells before and after the phase transition. The vertical black line indicates the target operating wavelength λ = 1064 nm of our optical limiters. Every designs use reference wavelength λ0 = 750 nm.

## 2.5 Fabry–Pérot cavity design for absorptive film (remove this part?)

In all the previously discussed designs, both phases of Sb2Se3 exhibits little to no absorption at λ = 1064 nm. But its extinction coefficients at 532 nm are significant, 1.09 and 2.24 for amorphous and crystalline Sb2Se3, respectively. The effect extinction coefficient has on absorption can be explained using the same single-layer Sb2Se3 design with HWOT thickness deposited on SiO2 substrate shown previously, an antireflection condition only occurs when both reflected R1 and R2 light have the same amplitude but a phase difference of π radian. If the material has non-zero k, some of the transmitted light will be absorbed and converted to thermal energy, which means the amplitude of R1 will be reduced. This can be visualized by plotting the effective reflective index (nr) from Eq. 4 as a function of phase thickness (θ) from Eq. 5 to create a contour graph [39], the x-axis represents the refractive index of the structure, while the y-axis represent its phase thickness, and the starting point is the refractive index of substrate (nsubstrate = nSiO2 = 1.47). To create an antireflection condition, the ending point should come back to the starting point (or for a perfect AR, the ending point should be the incident medium, air). Figure 7 compares a HWOT-thick Sb2Se3 design (ñSbSe = 3.96 + 1.09i at 532 nm) to an ideal film with the same n-index but has zero k (ñimag = 3.96 + 0.00i). The contour graphs are shown in Fig. 7a. with nSiO2 = 1.47 + 0i as the starting point, only when k is zero can the contour line return to the starting point.

Fig. 7. Comparison between Sb2Se3 (solid) and an ideal lossless-film with the same n-index (dotted). (a) Effective reflective index (nr) when θ = π radian (HWOT); only the contour line of lossless film returns to the starting point, creating an antireflection condition. (b) Even though both designs use the same λ0 = 532 nm, only lossless film reaches the lowest reflectance at λ0, reflectance of Sb2Se3 increased and the minimum point red-shifted to 594 nm.

A Fabry–Pérot cavity design can be used to enhance the absorption of the middle layer (PCM) while also reducing the total middle layer thickness [40]. The cavity consists of the PCM layer in the center and distributed Bragg reflectors on top and bottom of PCM. The two reflectors function as mirrors that cause light to cycle through the central PCM layer multiple times, this effectively reduce the required PCM thickness. This benefit is especially useful for PCM with high Ttrans such as Sb2Se3 because it lowers the energy requirement to start phase transition, and reduces damage caused by partial phase transition in thick PCM [17, 32]. The mirror structure can be viewed as a unit cell (U) composed of high (H) and low (L) refractive index materials with QWOT. The optical enhancement is directly correlated to the refractive index contrast between H and L. The unit cell is denoted as U = (H2LH2), as described earlier. The resonant condition in Fabry–Pérot design can be simplified into a simpler optically equivalent layer. For example, a symmetrical cavity with H as central layer and U1 on both sides (U1 C U1) can be written as:

H2LH2HH2LH2,						(19)

the two H2 and H layer in the middle are combined into (H H), which create HWOT-thick H layer with a 2π optical path different, equivalent to a transparent layer. So, Eq. 19 become:

H2 L L H2,							(20)

again, the (L L) layer in the middle combine into a HWOT-thick L film. This leaves two H2 layers, which combine to a single QWOT-thick H layer.

H2 H2,						(21)

H.						(22)

But an AR design with nH > nsubstrate require an H-layer thickness be increased to HWOT, this can be accomplished by adding H2 layer to the leftmost and rightmost position in Eq. 19:

H2H2LH2HH2LH2H2.					(23)

Eq. 23 is equivalent to (H H) layer which satisfy the condition for AR property. In reality, the middle can be changed to Sb2Se3, and the loss of resonance due to absorption can be compensated by changing the structure to have an additional layer(s) at the middle while also reduce the number of unit cell on the incident side to create asymmetrical reflectors [40].

# 3. Methods

## 3.1 Optical limiter design

In this work, we will use transfer matrix method (TMM) of Fresnel equation to calculate the transmittance, absorptance and reflectance of each design. In some simulation works, the substrate index can consider to be equal to air (nsub = nair = 1.0) to simplify the design and allows for a more widely applicable analysis methods, but in this work we choose to simulate 3-mm thick silica (SiO2) as substrate with refractive index data from [47], its refractive index is around 1.47 at both 1064 and 532 nm wavelengths. The H layers are Si [48], TiO2 [43] and Si3N4 [46]. The L layers are Al2O3 [43], SiO2 and MgF2 [42]. All the above mentioned material refractive indices can be found on refractiveindex.info website [49], but since antimony triselenide (Sb2Se3) is a relatively new material in the field of optics, its refractive index couldn’t be found there. We use dataset from [22], as shown in Fig. 1. The refractive index of air is set na = 1.0 across the spectra. The incident angle is 0° and light is transverse electric (TE) polarized for all calculations.

Our optical limiters are designed will either be designed for 1064 or 532 nm wavelengths. For 1064-nm devices, the designs are single-layer, multi-layer, and edge-filter. The goals are to design a broadband optical limiter with large transmission contrast (ΔT) between the two modes. Because of the low absorption caused by near-zero k-index in both phases at this wavelength, the devices cannot be self-activated. But since Sb2Se3 have high extinction coefficients at 532-nm wavelength, ka = 1.09 and kc = 2.24, we will compare simple design approaches (e.g., single or multi-layer designs) to asymmetrical cavity design. The goal is to create self-activating optical limiters and show their transmission, absorption, PCM used, and overall device thickness.

## 3.2 Simulation of endurance and optical stability under large phase switching cycles

Experimental studies have demonstrated that Sb2Se3 can have phase switching cycles with minimal degradation to its optical contrast up, and maintain a low-loss, reversible modulation in an order of 106 cycles [32]. Even so, Sb2Se3 still exhibits slight complex refractive index drift due to structural relaxation and cumulative thermal damage. Accounting for these variations is essential for ensuring long-term reliability and precision in high-endurance photonic applications [32, 33]. To account for this, the complex refractive index (ñ) can  be rewritten from Eq. 1 as:

npN=npN+ikpN	,					(24)

where N is the number of phase switching cycle.

The real part of the refractive index (n) is described by an exponential relaxation towards a saturated value such that:

npN=np,∞-np,∞-np,0exp-αpN,				(25)

where np,∞ is the asymptotic index after many cycles, np,0 is the refractive index at the first cycle (obtained from ellipsometry or literature data), and αp is the drift coefficient per cycle of phase p [22, 50].

Meanwhile, the imaginary part (k) can be approximated from a linear growth as:

kpN=kp,0(1+βpN),						(26)

where kp,0 is the initial loss and βp is the loss growth coefficient. The parameter βp is the relative loss per cycle of phase p [32, 51]. These models from Eq. (XXA) and (XXB) are adopted in this work, they are consistent with experimental trends and with general PCM endurance theory, providing a practical way to assess contrast degradation and threshold drift of PCM-based optical limiters over large cycles [22, 32, 50-52].

The endurance of optical limiters can be quantified using the following metrics: 1) transmitting contrast degradation, and 2) insertion loss.

#### Transmittance Contrast Degradation:

Degradation is defined as the reduction in transmittance contrast after N cycles, as in:

D(N)=ΔT(N)-ΔT0ΔT0, 					(27)

where transmittance contrast ΔT0 is the difference between amorphous (ON) and crystalline (OFF) phases at the initial cycle (N = 0).

ΔTN=TaN- TcN.					(28)

#### Insertion loss:

The insertion loss of the device at cycle N compares it transmittance to a reference state of cycle 0 [53], such that: Tc(1) or Tc(0)?

ILdBN=10logTc(N)Tc(1).					(29)

A growing IL(N) indicates increasing loss, typically driven by the linear growth of the imaginary index kp(N) and by detuning of the resonance due to drift of np(N).

# 4. Results & Discussions

## 4.1 Optical properties of 1064-nm optical limiters

Antimony triselenide shows zero extinction coefficient in the infrared spectra of amorphous phase, so an ideal limiter could have a perfect 100% transmittance in ON mode. The number of layers, Sb2Se3 needed for the entire structure, overall device thickness, transmittance in each mode, and transmittance contrast (ΔT) of each design are shown in Table 1. Aside from the single-layer design, only edge-filter designs and 3 unit-cell Fabry-Perot design show transmission contrast higher than 50%. The 5-unit-cells edge-filter design has the highest transmission contrast at 93.4%. It should be noted that there is only marginal improvement in ΔT of 0.7% when increasing the number of unit cells from 4 to 5 in an edge-filter design but the device thickness is increase by 25%. And although the 3-unit-cells Fabry-Perot designs use thinner Sb2Se3 layer than any other designs, which should reduce the energy required for phase transition, its overall device size is unreasonably large at more than 2 µm.

Table 1. Designs of 1064-nm Sb2Se3-based optical limiter. Transmission is calculated at λ = 1064 nm. Single, two, and three-layer designs all have λ0 = 1064 nm, but edge-filter designs have λ0 = 750 nm.

| Design | Layout | Number of layers | SbSe used (nm) | Device size (nm) | T (ON) (%) | T (OFF) (%) | ΔT (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Single-layer | SbSe | 1 | 157.9 | 157.9 | 93.5 | 37.2 | 56.3 |
| Two-layer | SbSe/TiO | 2 | 78.9 | 194.1 | 93.3 | 76.9 | 16.4 |
| Three-layer | SbSe/MgF/TiO | 3 | 78.9 | 580.3 | 93.3 | 76.9 | 16.4 |
| Three-layer | SiN/SbSe/AlO | 3 | 157.9 | 455.7 | 96.6 | 83.3 | 13.3 |
| Edge filter | (SbSe2/MgF/SbSe2)1 | 3 | 49.5 | 185.3 | 93.3 | 50.1 | 43.2 |
| Edge filter | (SbSe2/MgF/SbSe2)2 | 5 | 99.0 | 370.7 | 93.1 | 13.3 | 79.8 |
| Edge filter | (SbSe2/MgF/SbSe2)3 | 7 | 148.5 | 556.0 | 93.0 | 2.9 | 90.1 |
| Edge filter | (SbSe2/MgF/SbSe2)4 | 9 | 198.0 | 741.3 | 93.3 | 0.6 | 92.7 |
| Edge filter | (SbSe2/MgF/SbSe2)5 | 11 | 247.5 | 926.7 | 93.5 | 0.1 | 93.4 |
| Edge filter | (SbSe2/MgF/SbSe2)6 | 13 | 296.9 | 1,112.0 | 93.3 | 0.0 | 93.3 |
| Fabry-Perot | U1 SbSe/TiO U1 | 7 | 31.6 | 815.3 | 96.6 | 83.7 | 12.9 |
| Fabry-Perot | U3 SbSe/TiO U3 | 15 | 32.0 | 2071.3 | 96.5 | 11.7 | 84.8 |

Figure 8 is a comparison of transmittance contrast (ΔT) between the single-layer HWOT design and various edge-filter design. Even though all edge-filter designs use the same λ0 = 750 nm, not all designs have the highest ΔT at exactly 1064 nm. The 5 and 6 unit-cells (yellow and red colours, respectively) have a high ΔT for wider wavelengths, so they would be better suited to a broad spectrum use case than 4 unit-cells design.

Fig. 8. Transmittance contrast comparison of the design shown in Table 1. The reference wavelength (λ0) of the single-layer design is 1064 nm. All edge-filters designs have λ0 = 750 nm.

An edge-filter design required multiple layers of Sb2Se3, this would complicate the setup for phase switching. And if laser induced heating is used as a switching method, the phase transition of every Sb2Se3 layer will not occur simultaneously such that the transmission will changes in a gradual manner. This effect is seen in Sarangan, et al. [4]’s work, their self-activating optical limiter use the same long-pass edge-filter (H2LH2)4 design but changes H layer from GST to Sb2Se3, and change L layer from SiO2 MgF2 instead. Their experimental result shows that the phase switching of GST layers happens layer-by-layer in a sequence that is determined by the changes in optical field distribution and thermal crosstalk between layers.

Other criteria that have not been considered yet is the optical properties at different incident angles. Figure 9 shows the transmittance contrast of 4-unit-cells edge-filter design with incident angles ranging from 0 to 90 degrees, the light is TE (Fig.9a) and TM (Fig.9b) polarized. For TE polarized light, the transmittance contrast remains higher than 80% for up to 45°. The spectral edge of both type of polarization remains the same at any angle.

Fig. 9. Heatmaps showing transmittance contrast of incident light with varying wavelength and incident angle of the 4-unit-cell edge-filter design shown in Table 1. Incident light is (a) TE and (b) TM polarized.

To compare the optical performance of Sb2Se3-based edge-filter design to other PCM-based design, such as GST or VO2, we first need to consider their complex refractive index. Both GST and VO2 has a large extinction coefficients (imaginary part; k) at 1064-nm; kGST(amo) = 0.49 and kVO2(insulator) = 0.48, so the total PCMs used in a design will be the main limitation. A single-layer QWOT-thick (60.0 nm) GST already has absorptance value as high as 66.1%, which means a single-layer HWOT, multi-layer, or edge-filter GST or VO2-based designs will have very low transmission in ON mode. So, we choose asymmetrical resonant cavity designs for these two PCM for comparison. Table 2 is the transmission contrast comparison of different PCM-based 1064-nm optical limiters, which are Sb2Se3, GST [54], and VO2 [55].

The Sb2Se3-based optical limiters still have highest transmittance contrast.

## 4.2 Endurance simulation of 1064-nm optical limiters

The endurance and optical stability of a single-layer, and edge filter with number of unit cells N = 4 are shown in Fig. 9. Thickness of Sb2Se3 used in single-layer design is 157 nm (HWOT) which is thicker than 79 nm (QWOT) Sb2Se3 layer used in a two-layer SbSe/TiO design. This shows comparable optical stability. When Sb2Se3 is segmented into a thinner layer in an edge-filter design, its optical stability is still comparable, even though the overall Sb2Se3 used is greater.

The endurance testing of 1064-nm limiters, as shown in figures 9-11, confirms that all three designs, single Sb2Se3 layer, Sb2Se3 bilayer, and 11-layers-edge-filter cavity remain functional up to 1.5×10⁶ thermos-optical cycles, with gradual but design-dependent degradation of their key figures of merit.

For the single-layer HWOT optical limiter (Fig. 9), the amorphous-phase transmittance (ON mode) stays high and nearly constant over most of the cycling window, whereas the crystalline-phase transmittance (OFF mode) slowly increases with cycle number, indicating a reduction of effective phase contrast in the film. The addition of TiO2 layer in two-layer limiter (Fig. 10) slightly modifies the absolute transmittance levels but preserves the same qualitative trend of stable high-transmission amorphous phase and slowly brightening crystalline phase. In the 11-layer-edge-filter cavity optical limiter (Fig. 11), both phases show more pronounced evolution because the resonance is more sensitive to small index drifts, yet the device still maintains a clear separation between amorphous and crystalline transmission after 1.5×10⁶ cycles.

The normalized contrast decreases monotonically with cycle number for all structures. The single-layer design exhibits the slowest contrast decay, consistent with its simpler interference condition and weaker field enhancement. In contrast, the multilayer cavity shows a faster reduction of normalized contrast, reflecting the stronger dependence of the resonant line shape on endurance-induced changes in the Sb2Se3 refractive index and loss.

When the contrast change is expressed as percentage degradation relative to the first cycle (N = 0), all devices show only modest loss at low cycle counts and a more rapid decline as the test approaches 1.5×10⁶ cycles. The two-layer and edge-filter cavity structures display larger percentage degradation than the single-layer limiter, which indicates that while resonant enhancement improves low-cycle performance, it also amplifies the impact of long-term refractive index drift in phase change material.

Finally, the insertion loss in the high-transmission amorphous phase increases gradually with cycling number for every structures, reflecting the small but cumulative rise in absorption and scattering limits for 1064-nm operation, especially for the single and two-layer designs. This imply that endurance-induced losses do not fully compromise the limiter performance over a targeted lifetime.

## 4.3 Suggestions and limitation

The backside reflection from the substrate-air layer (Rb) creates a slight reflectance. A single layer of MgF2 deposited on the bottom of the substrate can reduce this effect. This reflection can simply be reduced by applying a translucent adhesive tape to the bottom of the substrate, which create a scattering effect [56].

To further increase the optical performance, a simple optimization scheme, such as merit function found in OpenFilters [57], can be used to reduce the reflectance in the ON mode by varying the thickness of each layer. We set the function to optimize our 4-unit-cells edge-filter design for lowest reflectance at λ = 1000, 1100 and 1200 nm. Figure XX shows the transmission contrast of the optimized 4-unit-cells compared to the standard 4-unit-cells edge-filter design.

Our work still lacks thermal analysis which would determine the intensity of laser and pulse duration required for phase switching of both 532 and 1064 nm optical limiters.

Future research should be focus on thermal simulation or real-world fabrication. The latter is especially encouraged since further complication that can’t be accounted in a simulation, such as thickness control and materials limitation in each deposition method, could be the most important criteria in design selection.

# 5. Discussions

Figure XX shows the heatmap of transmittance contrast from 4-unit-cells edge-filter design with incident angles ranging from 0 degrees to 90 degrees. Where X-axis is still the wavelength and Y-axis is changed to the incident angle.

Finite Element Method (FEM) [6]

For a self-activating optical limiter at 532 nm, resonance can be restored with asymmetrical designs. Asymmetrical cavity designs required thinner Sb2Se3. Which should prevent partial phase-transition described in [32]. The question then becomes ‘at what threshold of laser intensity will the optical limiter be turned off? If the threshold is low, then the device needs to have more absorptivity in the ON mode. But if the threshold is high, then the absorptivity in the ON mode does not need to be as high. Its absorptivity in the OFF mode is also important; it ideally should be as high as possible since it need to be re-amorphized at an even higher temperature to return the device from OFF to ON mode. Would a volatile-type PCM be more suitable for self-activating optical limiter?

# 6. Conclusions

We have shown that Sb2Se3 can be used as a high-efficient, broadband optical limiter in 1064 nm wavelength. Long-pass edge-filter designs with Sb2Se3 as H and MgF2 as L layers have the best performance, and edge-filter design with unit-cell numbers greater than 3 show transmittance contrast above 90%. Design with 4 unit cells have transmission contrast of 92.7% and is 741.3 nm thick.

It cons are the overall thicker Sb2Se3 needed for the design, and higher number of layers result in more complicated fabrication. Inducing phase transition is also more complicated in a multi-layer designs.

Fabry–Pérot design allows for the restoration of resonance condition in material with non-zero extinction coefficient, such as Sb2Se3 at 532 nm. The design use thinner Sb2Se3 than a simple single, multi-layer, or edge-filter designs but its limitations are the narrower operating bandwidth, and the difficulty of fabricating multiple film layers with tight thickness tolerance.

Optimization using computer has a significant impact on the overall performance, OpenFilters or similar program should be used after the initial design.

# 7. Acknowledgement

# Note

Opt. Commun.

Opt. Laser Technol.

สอบหัวข้อ: Ratchapak Chitaree, Witoon Yindeesuk, Prathan Buranasiri. วันอังคารที่ 9 มิถุนายน เช้า

Note:

1550:

MgF2:	1.3746		[42]

SiO2: 	1.4443		[47]

Al2O3: 	1.6141		[43]

Si3N4: 	1.9904		[46]

TiO2:	2.2899		[43]

Vo2:	2.8593+0.2811i	(1.6077+2.7221)	 [55]

Sb2Se3:	3.2854 (4.0499)	[22]

Si_cry_300k:	3.4795	[45]

Si_amo_20deg: 	3.7771	[48]

GST:	4.0736+0.0092	(6.4644 +0.919802i) [54]

1064:

MgF2:	1.3777		[42]

SiO2: 	1.4671		[47]

Al2O3: 	1.6165+0i	[43]

Si3N4: 	1.9966+0i	[46]

TiO2:	2.3097		[43]

Vo2:	2.7486+0.4784	(1.3346+1.4580)	 [55]

Sb2Se3:	3.369674+0i (4.3081+0.009744i)	[22]

Si_cry_300k:	3.5552	[45]

Si_amo_20deg: 	3.9017	[48]

GST:	4.4376+0.49271i	(6.0744+2.454029i) [54]

532:

MgF2:	1.3842		[42]

SiO2: 	1.4754		[47]

Al2O3: 	1.6311+0i	[43]

Si3N4: 	2.0341+0i	[46]

TiO2:	2.4503		[43]

Vo2:	2.7680+0.6673	(2.4835+0.6618)	 [55]

Sb2Se3:	3.9615+1.093042i (4.7876+2.240748i)	[22]

Si_cry_300:	4.1473+0.039769i	[45]

`	Si_amo_20deg:	4.9143+0.66141i		[48]

# 8. References

[1]	K. Matuszek, M. Kar, J. M. Pringle, and D. R. MacFarlane, "Phase Change Materials for Renewable Energy Storage at Intermediate Temperatures," Chemical Reviews, vol. 123, no. 1, pp. 491–514, 2023/01/11 2023, doi: 10.1021/acs.chemrev.2c00407.

[2]	R. Matos and N. Pala, "A Review of Phase-Change Materials and Their Potential for Reconfigurable Intelligent Surfaces," Micromachines, vol. 14, no. 6, p. 1259, 2023. [Online]. Available: https://www.mdpi.com/2072-666X/14/6/1259.

[3]	U. Biswas, S. A. Chanu, S. Alam, A. Ashraf, and R. K. Sonkar, "Design of Optical Limiter Using Nonlinear Kerr Effect for the “Far Ultraviolet-C” Band," in 2025 IEEE Photonics Conference (IPC), 9–13 Nov. 2025 2025, pp. 1–2, doi: 10.1109/IPC65510.2025.11281888. [Online]. Available: https://ieeexplore.ieee.org/stampPDF/getPDF.jsp?tp=&arnumber=11281888&ref=

[4]	A. Sarangan, J. Duran, V. Vasilyev, N. Limberopoulos, I. Vitebskiy, and I. Anisimov, "Broadband Reflective Optical Limiter Using GST Phase Change Material," IEEE Photonics Journal, vol. 10, no. 2, pp. 1–9, 2018, doi: 10.1109/jphot.2018.2796448.

[5]	C. Wan et al., "Ultrathin Broadband Reflective Optical Limiter," Laser & Photonics Reviews, vol. 15, no. 6, p. 2100001, 2021, doi: https://doi.org/10.1002/lpor.202100001.

[6]	X. Ling, X. Pang, X. Chen, and Z. Shao, "Broadband mid-infrared optical limiter based on&#x00A0;vanadium dioxide phase transition," J. Opt. Soc. Am. B, vol. 42, no. 9, pp. 2062–2067, 2025/09/01 2025, doi: 10.1364/JOSAB.569492.

[7]	M. Gandolfi et al., "Optical Limiting Thin Multilayer Films Based On Phase Transition In VO2," in 2022 Sixteenth International Congress on Artificial Materials for Novel Wave Phenomena (Metamaterials), 12–17 Sept. 2022 2022, pp. 148–150, doi: 10.1109/Metamaterials54993.2022.9920767. [Online]. Available: https://ieeexplore.ieee.org/stampPDF/getPDF.jsp?tp=&arnumber=9920767&ref=

[8]	A. Tognazzi et al., "Opto-thermal dynamics of thin-film optical limiters based on the VO2 phase transition," Opt. Mater. Express, vol. 13, no. 1, pp. 41–52, 2023/01/01 2023, doi: 10.1364/OME.472347.

[9]	A. Donval, Y. Ofir, D. Nevo, and M. Oron, "Reflective Optical Limiter," US Patent US 2014/0233085 A1 Patent Appl. US 201214343922 A, 2014/08/21, 2014. [Online]. Available: https://lens.org/107-268-237-474-798

[10]	A. N. H. Lam Tai, "OPTICAL LIMITERS FOR FACILITATING APERTURE PROTECTION," US Patent US 2019/0094430 A1 Patent Appl. US 201715716364 A, 2019/03/28, 2019. [Online]. Available: https://lens.org/168-829-457-144-045

[11]	W. Jia, R. Menon, and B. Sensale-Rodriguez, "Unique prospects of phase change material Sb2Se3 for ultra-compact reconfigurable nanophotonic devices," Opt. Mater. Express, vol. 11, no. 9, pp. 3007–3014, 2021/09/01 2021, doi: 10.1364/OME.435979.

[12]	P. Xu, J. Zheng, J. K. Doylend, and A. Majumdar, "Low-Loss and Broadband Nonvolatile Phase-Change Directional Coupler Switches," ACS Photonics, vol. 6, no. 2, pp. 553–557, 2019/02/20 2019, doi: 10.1021/acsphotonics.8b01628.

[13]	Y. Zhang et al., "Broadband transparent optical phase change materials for high-performance nonvolatile photonics," Nature Communications, vol. 10, no. 1, p. 4279, 2019/09/30 2019, doi: 10.1038/s41467-019-12196-4.

[14]	H. Li, D. Zeng, Y. Huang, Q. Huang, and X. Zhang, "Ultra-compact, ultra-low-loss and broadband 2 x 2 nonvolatile optical switch based on Sb(2)Se(3) phase change material," Opt Express, vol. 32, no. 20, pp. 35287–35297, Sep 23 2024, doi: 10.1364/OE.534645.

[15]	D. d. Ceglia, M. Grande, A. Vincenti, C. Baratto, and C. d. Angelis, "Tunable Filters for Visible Light Based on Resonant VO2 Planar Thin Films," in 2020 22nd International Conference on Transparent Optical Networks (ICTON), 19–23 July 2020 2020, pp. 1–4, doi: 10.1109/ICTON51198.2020.9203244.

[16]	R. Heenkenda, K. Hirakawa, and A. Sarangan, "Tunable optical filter using phase change materials for smart IR night vision applications," Opt. Express, vol. 29, no. 21, pp. 33795–33803, 2021/10/11 2021, doi: 10.1364/OE.440299.

[17]	Y.-S. Huang et al., "Tunable structural transmissive color in fano-resonant optical coatings employing phase-change materials," Materials Today Advances, vol. 18, p. 100364, 2023/06/01/ 2023, doi: https://doi.org/10.1016/j.mtadv.2023.100364.

[18]	C. Wan et al., "Limiting Optical Diodes Enabled by the Phase Transition of Vanadium Dioxide," ACS Photonics, vol. 5, no. 7, pp. 2688–2692, 2018/07/18 2018, doi: 10.1021/acsphotonics.8b00313.

[19]	H. Kocer et al., "Intensity tunable infrared broadband absorbers based on VO2 phase transition using planar layered thin films," Scientific Reports, vol. 5, no. 1, p. 13384, 2015/08/21 2015, doi: 10.1038/srep13384.

[20]	X. Tian and Z.-Y. Li, "An Optically-Triggered Switchable Mid-Infrared Perfect Absorber Based on Phase-Change Material of Vanadium Dioxide," Plasmonics, vol. 13, no. 4, pp. 1393–1402, 2018/08/01 2018, doi: 10.1007/s11468-017-0643-9.

[21]	C. Liu et al., "Tunable nonlinear optical absorption in amorphous and crystalline Sb2Se3 thin films," Journal of Alloys and Compounds, vol. 791, pp. 753–760, 2019/06/30/ 2019, doi: 10.1016/j.jallcom.2019.03.295.

[22]	M. Delaney, I. Zeimpekis, D. Lawson, D. W. Hewak, and O. L. Muskens, "A New Family of Ultralow Loss Reversible Phase‐Change Materials for Photonic Integrated Circuits: Sb2S3 and Sb2Se3," Advanced Functional Materials, vol. 30, no. 36, 2020, doi: 10.1002/adfm.202002447.

[23]	Z. Gong et al., "Phase change materials in photonic devices," Journal of Applied Physics, vol. 129, no. 3, 2021, doi: 10.1063/5.0027868.

[24]	A. A. Burtsev et al., "Physical properties’ temperature dynamics of GeTe, Ge2Sb2Te5 and Ge2Sb2Se4Te1 phase change materials," Materials Science in Semiconductor Processing, vol. 150, p. 106907, 2022/11/01/ 2022, doi: https://doi.org/10.1016/j.mssp.2022.106907.

[25]	P. Guo, Z. Biegler, T. Back, and A. Sarangan, "Vanadium dioxide phase change thin films produced by thermal oxidation of metallic vanadium," Thin Solid Films, vol. 707, p. 138117, 2020/08/01/ 2020, doi: https://doi.org/10.1016/j.tsf.2020.138117.

[26]	M. E. A. Warwick and R. Binions, "Advances in thermochromic vanadium dioxide films," Journal of Materials Chemistry A, 10.1039/C3TA14124A vol. 2, no. 10, pp. 3275–3292, 2014, doi: 10.1039/C3TA14124A.

[27]	Y. Cui et al., "Thermochromic VO2 for Energy-Efficient Smart Windows," Joule, vol. 2, no. 9, pp. 1707–1746, 2018/09/19/ 2018, doi: https://doi.org/10.1016/j.joule.2018.06.018.

[28]	J. Sang et al., "Smart Windows with a VO2 Thin Film as a Conductive Layer for Efficient and Independent Dual-Band Modulation," ACS Applied Electronic Materials, vol. 3, no. 11, pp. 4882–4890, 2021/11/23 2021, doi: 10.1021/acsaelm.1c00728.

[29]	N. Murillo-Quirós, V. Vega-Garita, A. Carmona-Calvo, E. A. Rojas-González, R. Starbird-Perez, and E. Avendaño-Soto, "Toward Thermochromic VO2 Nanoparticles Polymer Films Based Smart Windows Designed for Tropical Climates," Polymers, vol. 14, no. 19, p. 4250, 2022. [Online]. Available: https://www.mdpi.com/2073-4360/14/19/4250.

[30]	X. Chen, J. Lin, and K. Wang, "A Review of Integrated Photonic Devices Using Sb2Se3," Advanced Physics Research, vol. 4, no. 1, p. 2400080, 2024, doi: 10.1002/apxr.202400080.

[31]	C. Chen et al., "Optical properties of amorphous and polycrystalline Sb2Se3 thin films prepared by thermal evaporation," Applied Physics Letters, vol. 107, no. 4, 2015, doi: 10.1063/1.4927741.

[32]	D. Lawson, S. Blundell, M. Ebert, O. L. Muskens, and I. Zeimpekis, "Optical switching beyond a million cycles of low-loss phase change material Sb2Se3," Opt. Mater. Express, vol. 14, no. 1, 2023, doi: 10.1364/ome.509434.

[33]	M. S. Alam et al., "Fast Cycling Speed with Multimillion Cycling Endurance of Ultra-Low Loss Phase Change Material (Sb2Se3) by Engineered Laser Pulse Irradiation," Advanced Functional Materials, vol. 34, no. 14, p. 2310306, 2024, doi: https://doi.org/10.1002/adfm.202310306.

[34]	J. Faneca et al., "Towards low loss non-volatile phase change materials in mid index waveguides," Neuromorphic Computing and Engineering, vol. 1, no. 1, p. 014004, 2021/08/23 2021, doi: 10.1088/2634-4386/ac156e.

[35]	S. Blundell et al., "Ultracompact Programmable Silicon Photonics Using Layers of Low-Loss Phase-Change Material Sb2Se3 of Increasing Thickness," ACS Photonics, vol. 12, no. 3, pp. 1382–1391, 2025/03/19 2025, doi: 10.1021/acsphotonics.4c01789.

[36]	J. H. Vella et al., "Experimental Realization of a Reflective Optical Limiter," Physical Review Applied, vol. 5, no. 6, p. 064010, 06/20/ 2016, doi: 10.1103/PhysRevApplied.5.064010.

[37]	C. Baratto et al., "Optical Limiting Sensor Based on Multilayer Optimization of Ag/VO2 Phase Change Material," IEEE Sensors Letters, vol. 7, no. 9, pp. 1–3, 2023, doi: 10.1109/LSENS.2023.3300801.

[38]	L. Shah, S. Cannon Roger, and A. Drummer Mark, "LIDAR RECEIVER OPTICAL LIMITER," US Patent US 2025/0172672 A1 Patent Appl. US 202418960941 A, 2025/05/29, 2025. [Online]. Available: https://lens.org/118-293-389-504-62X

[39]	A. Sarangan, Optical Thin Film Design, 1st Edition ed. Boca Raton: CRC Press, 2020.

[40]	A. Sarangan, "Design of resonant cavity thin film structures with complex active layers," J. Opt. Soc. Am. B, vol. 37, no. 11, pp. 3461–3468, 2020/11/01 2020, doi: 10.1364/JOSAB.404894.

[41]	L. Gao, F. Lemarchand, and M. Lequime, "Exploitation of multiple incidences spectrometric measurements for thin film reverse engineering," Opt. Express, vol. 20, no. 14, pp. 15734–15751, 2012/07/02 2012, doi: 10.1364/OE.20.015734.

[42]	D. Franta, D. Nečas, A. Giglia, P. Franta, and I. Ohlídal, "Universal dispersion model for characterization of optical thin films over wide spectral range: Application to magnesium fluoride," Applied Surface Science, vol. 421, pp. 424–429, 2017/11/01/ 2017, doi: https://doi.org/10.1016/j.apsusc.2016.09.149.

[43]	S. V. Zhukovsky et al., "Experimental Demonstration of Effective Medium Approximation Breakdown in Deeply Subwavelength All-Dielectric Multilayers," Physical Review Letters, vol. 115, no. 17, p. 177402, 10/23/ 2015, doi: 10.1103/PhysRevLett.115.177402.

[44]	Y. Li et al., "Preparation of mechanically stable triple-layer interference broadband antireflective coatings with self-cleaning property by sol–gel technique," RSC Advances, 10.1039/C7RA00844A vol. 7, no. 24, pp. 14660–14668, 2017, doi: 10.1039/C7RA00844A.

[45]	D. Franta, P. Franta, J. Vohánka, M. Čermák, and I. Ohlídal, "Determination of thicknesses and temperatures of crystalline silicon wafers from optical measurements in the far infrared region," Journal of Applied Physics, vol. 123, no. 18, 2018, doi: 10.1063/1.5026195.

[46]	L. Y. Beliaev, E. Shkondin, A. V. Lavrinenko, and O. Takayama, "Optical, structural and composition properties of silicon nitride films deposited by reactive radio-frequency sputtering, low pressure and plasma-enhanced chemical vapor deposition," Thin Solid Films, vol. 763, p. 139568, 2022/12/01/ 2022, doi: https://doi.org/10.1016/j.tsf.2022.139568.

[47]	D. Franta, D. Nečas, I. Ohlídal, and A. Giglia, Optical characterization of SiO2 thin films using universal dispersion model over wide spectral range (SPIE Photonics Europe). SPIE, 2016.

[48]	O. C. Karaman, G. N. Naidu, A. R. Bowman, E. N. Dayi, and G. Tagliabue, "Decoupling Optical and Thermal Dynamics in Dielectric Metasurfaces for Self-Encoded Photonic Control," Laser & Photonics Reviews, vol. 19, no. 24, p. e01014, 2025, doi: https://doi.org/10.1002/lpor.202501014.

[49]	M. N. Polyanskiy, "Refractiveindex.info database of optical constants," Scientific Data, vol. 11, no. 1, p. 94, 2024/01/18 2024, doi: 10.1038/s41597-023-02898-2.

[50]	L. Martin-Monier et al., "Endurance of chalcogenide optical phase change materials: a review," Opt. Mater. Express, vol. 12, no. 6, pp. 2145–2167, 2022/06/01 2022, doi: 10.1364/OME.456428.

[51]	Y. Zhang et al., "Myths and truths about optical phase change materials: A perspective," Applied Physics Letters, vol. 118, no. 21, 2021, doi: 10.1063/5.0054114.

[52]	S. Kim, G. W. Burr, W. Kim, and S.-W. Nam, "Phase-change memory cycling endurance," MRS Bulletin, vol. 44, pp. 710–714, September 01, 2019 2019, doi: 10.1557/mrs.2019.205.

[53]	R. Paschotta, Encyclopedia of Laser Physics and Technology. Wiley, 2008.

[54]	J. A. Frantz et al., "Optical constants of germanium antimony telluride (GST) in amorphous, crystalline, and intermediate states," Opt. Mater. Express, vol. 13, no. 12, pp. 3631–3640, 2023/12/01 2023, doi: 10.1364/OME.506019.

[55]	I. O. Oguntoye, S. Padmanabha, M. Hinkle, T. Koutsougeras, A. J. Ollanik, and M. D. Escarra, "Continuously Tunable Optical Modulation Using Vanadium Dioxide Huygens Metasurfaces," ACS Applied Materials & Interfaces, vol. 15, no. 34, pp. 41141–41150, 2023/08/30 2023, doi: 10.1021/acsami.3c08493.

[56]	R. Synowicki, "Suppression of backside reflections from transparent substrates," physica status solidi (c), vol. 5, pp. 1085–1088, 05/01 2008, doi: 10.1002/pssc.200777873.

[57]	S. Larouche and L. Martinu, "OpenFilters: open-source software for the design, optimization, and synthesis of optical filters," Appl. Opt., vol. 47, no. 13, pp. C219–C230, 2008/05/01 2008, doi: 10.1364/AO.47.00C219.