Note

Undecided

Check Ref.

Check logic

Design and Simulation of Sb2Se3-based Resonant Optical Limiters using Transfer Matrix Method

Surawut Wicharn1, Chettanat Padungatthakij2, Suebtarkul Suchat3, Nathan Hagen4, and Prathan Buranasiri2*

1 Department of Physics, Faculty of Science, Srinakharinwirot University, Bangkok, Thailand.

2 Department of Physics, School of Science, King Mongkut’s Institute of Technology Ladkrabang, Bangkok, Thailand.

3 Department of Physics, Faculty of Science and Technology, Phranakhon Rajabhat University, Bangkok, Thailand.

4 Department of Optical Engineering, Utsunomiya University, Tochigi, Japan.

* prathan.bu@kmitl.ac.th

# Abstract:

We proposed an optical limiter designs which utilize antimony triselenide (Sb2Se3). Optical limiter is a type of device that allows light to transmitted through in one mode, but can be switched off to block transmission. Sb2Se3 is a phase change material which has low loss in the IR spectrum, high and stable refractive index contrast in both visible and IR spectra, and a high phase switching endurance of up to an order of 106 cycles. Our optical limiters designs are for either 532 or 1064-nm usage; these two wavelengths have a distinctive design approaches, at 1064 nm Sb2Se3 has no absorption so it is suitable for a high efficiency optical limiters, but at 532 nm Sb2Se3 exhibits high absorption which complicated resonant design. Aside from the optical performance, we also investigate their optical endurance with computer simulations. (137 words)

Keywords: optical limiter, resonant cavity, Sb2Se3, phase change material  (keywords  < 7)

# 1. Introduction

Phase change material (PCM) can have different meanings depending on the field. In energy storage, the term would refer to material that store and release thermal energy through changes in its state of matter (latent heat), and the transition occurs between solid and liquid state [1]. However, in electronics and photonics, the term PCM refers to a solid-state material that changes its crystal structure, such as from amorphous to crystalline, when its temperature rise above transition temperature (Ttrans). The change in crystalline structure leads to a change in its optical properties, i.e. complex refractive index [2]. Complex refractive index comprises of real refractive index (n) and imaginary extinction coefficient (k) parts, and the refractive index contrast between the two phases of PCM is an order of magnitude larger than contrast induced by applied electric field or light intensity (Kerr effect) [3, 4]. This property makes PCM ideal for photonic applications that require the modulation of light transmittance, absorptance, or reflectance. Examples include optical limiters[4-10], optical switches[11-14], optical filters[15-17], optical diode[18], and absorbers[19-21].

Phase change material can be classified by its behavior after phase transition occurs. A volatile PCM will revert to its pre-transitioned phase when temperature drops below Ttrans. But non-volatile PCM will remain in its transitioned phase even after the temperature falls below Ttrans. To turn non-volatile PCM phase back to pre-transitioned phase, it needs to be heated above its melting temperature and then rapidly quenched. Examples of non-volatile PCMs are Ge2Sb2Te5 (GST) and Ge-Sb-Se-Te  (GSST). One of the earliest and most commonly studied non-volatile PCM is GST [22, 23]. It’s a chalcogenide glass that exhibits large refractive index contrast (n) between amorphous and crystalline phases. When compared to other non-volatile PCM, it has low Ttrans at ~145 °C for crystallization into cubical phase and changes into hexagonal phase at ~200 °C [4, 24]. Its drawback is the large extinction coefficient (k) in visible and IR spectrum, which causes high optical loss from absorption. Another popular non-volatile PCM is GSST (Ge2Sb2SexTex), it is a derivative of GST that substitutes some part of tellurium with selenium. It has a larger refractive index contrast in the visible spectrum like GST but has a lower extinction coefficient which improve optical efficiency. But GSST has higher Ttrans at ~242 °C [24]. In the past 10 years, VO2 gathered attention as a volatile PCM with Ttrans close to room temperature. It undergoes a metal-insulator transition (MIT) at Ttrans of 68 °C and has a relatively high refractive index contrast starting from near-IR (NIR) with small k in the insulating phase (low temperature). Its main drawbacks are its large k-index in the metallic phase [23] and noticeable thermal hysteresis [25]. Attempts have been made to reduce Ttrans of VO2 closer to room temperature, but these also reduce the switching endurance and refractive index contrast [26]. Beyond the above-mentioned applications, an example of VO2 usage is as thermochromic window coatings that helps with temperature regulation inside a room by blocking infrared sunlight in the summer, but allows light to come in during winter which helps with indoor heating [27-29].

Compared to other PCMs, antimony triselenide (Sb2Se3) is a relatively new material in the field of photonics, only one review paper existed prior to 2026 [30]. (recheck claims whether it’s still true). The initial researches on Sb2Se3 are in solar-energy applications [31], but Sb2Se3 has recently gathered interest as a non-volatile PCM for photonic applications [30] because of its near-zero extinction coefficient in the IR spectrum and beyond, its extinction coefficient is also lower than GST in the visible spectrum for both amorphous and crystalline phases, it has a relatively high and stable refractive index contrast from visible to IR spectrum, and has a fast switching time in a microsecond range [22, 32, 33]. The crystallization temperature of Sb2Se3 is between GST and GSST at ~186 °C [32]. It phase switching endurance is also high, at 4000 cycles [22], it also has been experimentally demonstrated to be as high as 106 to 107 cycles with an optimized laser-induced crystallization and re-amorphization schemes [32, 33]. These properties make Sb2Se3 attractive for a low-loss, reconfigurable optical switches and circuits that have been used in optical waveguide [11, 22, 34, 35]. Even so, to the best of our knowledge, Sb2Se3 applications as optical limiters have yet been explored.

Optical limiter is a photonic device that protects sensitive detector or eyes from high intensity light, it allows light to propagated through during its “ON” mode but will reflect or absorb light when switched to “OFF” mode. The device could be self-switching, i.e. undergoes a phase transition through light absorption [7, 8],  or it could switch its mode by external means, such as joule heating [16], or absorption of light outside of its intended operating bandwidth [32]. The device could either be designed to operate over a broad wavelengths [4-6, 36] or at a specific wavelength [7, 8, 37, 38]. An ideal optical limiter should maximize transmittance in the ON mode and minimizes it in the OFF mode, while also minimizing reflectance and absorptance in both modes. If it’s self-activating, it should have just enough absorption to induce phase transition. Optical limiter designs could be a planar thin-film structures or a nanostructured metasurfaces; planar structures are easier to design, optimize and fabricate, but metasurface structures offer more design flexibility [8]. For a planar designs, there are many ways to create high transmission such as 1) single or multi-layers antireflection (AR) designs and 2) Line-pass, long-pass, or short-pass filters [39]. All of these designs rely on resonance to achieve antireflection properties, but if the materials have high extinction coefficients (k), e.g. metals or some PCMs, the resonant condition will be disrupted due to energy loss associated with the thickness of high-k index film. Resonance can be restore by the use of asymmetrical resonant cavity [40], this design incorporates high k-index material placed between two mirror-like layers. The cavity designs also reducing the total thickness of PCM when compared to other designs, this is especially helpful in the case of volatile PCMs because it reduces the total energy required to induce phase transitions. Another benefit of using thinner PCM is the reduction of stress damage from the contraction and expansion in crystallization and re-amorphization processes [17]. It also reduce partial phase transition which happened when film size is above its thickness limit and open up more laser optimization schemes for inducing phase transitions [32].

In this work, we investigate Sb2Se3-based optical limiters with a planar thin-film designs. The reference wavelengths are selected to be 1064 or 532 nm because they are from Nd:YAG laser and its second harmonic which are commonly used in laboratory setups. Another reason is that the two wavelengths have a completely different design approaches. Near 1064 nm, Sb2Se3 has near-zero absorption in both phases and its refractive index contrast is stable throughout IR spectrum. The goal of the 1064-nm designs is to create a broadband (IR) optical limiter that have high transmission in the ON mode and reflected most of the light in the OFF mode. As for 532-nm designs, at this wavelength the k-index of Sb2Se3 are large for both amorphous and crystalline phases [22]. A simple AR, or a long/short-pass designs cannot achieve perfect antireflection conditions. Therefore, an asymmetrical resonant cavity design approach is used for 532-nm designs.

# 2. Theories

## 2.1 Optical Properties of Sb2Se3

The complex refractive index (ñ) of phase change material at any wavelength (λ) can be written as:

npλ=npλ+ikpλ						(1)

where the real term n is the refractive index, the imaginary term k is extinction coefficient, and p denotes the phase which for Sb2Se3 can either be amorphous (amo) or crystalline (cry). Dispersive models, such as Tauc-Lorentz or multi-oscillator fits are often used to represent the measured np and kp over the spectral range of interest. (need this part?). In this work, a linear interpolation is used since all the materials dataset used have the measurement interval of less than 4 nm. Figure 1 shows the complex refractive index of Sb2Se3 from 300-1700 nm using data from [22]. The blue line represents real refractive index (n), and the red line represents imaginary extinction coefficient (k). In amorphous phase (Fig. 1a), the refractive index increases from around 2.4 at 300 nm to a peak of around 4.0 at 600 nm and gradually decreases to a stable value of around 3.3 above 1200 nm, indicating a strong dispersion near the band edge of visible spectrum and a weaker dispersion in the NIR spectrum. The extinction coefficient starts at approximately 2.1 at 300 nm and dropped to zero at around 850 nm. In the crystalline phase (Fig. 1b), the refractive index is around the same value as that of amorphous phase but reached a peak of around 5.1 at around 660 nm, it is then dropped to a stable of 4.1 in the NIR spectrum. The k-index of crystalline phase peaked at around 3.1 in the near-UV spectrum and rapidly approach zero above 900 nm. So, antimony triselenide (Sb2Se3) refractive index contrast Δn = nc - na is large and stable in the visible through IR spectra, and extinction coefficients is very large in the near-UV but falls to zero around NIR spectrum for both phases, with crystalline phase exhibits higher absorption in the visible spectrum.

Fig. 1. Complex refractive index of Sb2Se3 in (a) amorphous, and (b) crystalline phases. The data are taken directly from [22].

## 2.2 Single-layer antireflection design

In designing optical limiters, we can first consider its optical performance in the ON mode first, and then consider its transmission contrast when switched to OFF mode. Most optical devices will either be optimized for antireflection (AR) or high reflection properties. But in this work, optical limiters is designed to utilize transmission and absorption only, minimizing reflection is beneficial (absorption is utilizes in phase transition).  The simplest thin-film device consists of a single film layer with no absorption deposit on a substrate. A single thin-film layer reflects light at two interfaces as shown in Fig. 2: the bottommost interface is between thin film and substrate (R1), and the topmost interface is air-film (R2). Antireflection condition occurs when destructive interference of R1 and R2 with the same amplitude and a phase difference of π radian (i.e. optical path length of λ/2) occurs. And since R1 travels through the film layer twice (transmitted down and reflected up), the film optical thickness only needs to be half of that, an optical thickness of λ/4 which also known as quarter-wave optical thickness (QWOT). Optical thickness (OT) is defined as the optical path length of wavelength (λ) through the film layer:

OT(λ)=n(λ)t,						(2)

where n is the refractive index of the film at λ, and t is the physical thickness of the film. For a single-layer AR device, the thin-film physical thickness (t) needs to be equal to:

t=OTn=λ04n.						(3)

Fig. 2. Light paths in a single-layer thin film device. R1 is the reflected light at the film-substrate interface, and R2 is the reflected light at the air-film interface. Antireflection occurs when the phase difference between the two is π radian. The reflection angles are exaggerated for illustration purpose; both angles are the same as incidents.

Another way to calculate the thickness required for AR condition is to consider the reflection of the device.  For a lone substrate with air as the initial incident medium, the reflectance (R) is related to Fresnel reflection coefficient (r) as the following:

R= r2=na-nsna+ns2,					(4)

where na is air refractive index, and ns is substrate refractive index. For single-layer film on a substrate, the combined film and substrate index is effective reflectance index (nr) [39]. It is defined as:

nr=nfns+nf+ns-nfe-i2θns+nf-ns-nfe-i2θ, 					(5)

where nf is the film refractive index, i denotes imaginary unit, and θ is the phase thickness which is related to optical thickness (OT) of the film by

θ=k0OT,						(6)

where k0 is the angular wavenumber (k0=2π/λ). By replacing ns with nr in Eq. 4, reflectance of a single-layer device become:

R=r2=na-nrna+nr2.					(7)

Antireflection condition is achieved when R = 0 or na = nr. This condition occurs when the phase thickness (θ) in Eq.5 is in multiple of π/2 radian, such as QWOT:

θ=Zπ2,							(8)

where Z can be any even integer. We can simplify Eq.5 using Euler’s identity (e-iπ = -1) to:

nr=nfns+nf-ns-nfns+nf+ns-nf=nf2ns,					(9)

so, an antireflection condition happen when nr = na or:

nans=nf2.						(10)

Another condition to consider is that the relative refractive index between air, film, and substrate must be such that nair < nf < nsubstrate. Reflected light shift its phase by π radian when reflected from lower to a higher refractive index medium. The reflected light (R2) at air-film interface undergoes π radian phase shift since nair is the lowest in most cases, so R1 must also has it phase shifted by the same amount. These two conditions place a limitation on material refractive index selection, since for a complete antireflection, there exist only one ideal answer for each substrate. Since the QWOT design must have film refractive index higher than air  but lower than substrate, which in this work is silica (SiO2), but Sb2Se3 has refractive index greater than silica at both 532 and 1064 nm wavelengths, the R1 light travelled 2QWOT = π radian further than R2 but only R2 has its phase shifted by π radian from reflection, so a constructive interference occurs instead. In this case, the film needs to be λ/2 or half-wave optical thick (HWOT) instead such that R1 would travel 2HWOT = 2π radian further than R2. As an example, at λ0 = 1064 nm, if we use 3-mm-thick SiO2 substrate with a refractive index of ns = 1.46 [41] the ideal film thickness needs to be QWOT and has a refractive index of 1.21 for a complete antireflection design. The value 1.21 is lower than any commonly available material and the material with the closest refractive index is MgF2 at 1.38 [42], this difference cause the reflection to be higher than an ideal film as can be seen in Fig. 3. In the case of Sb2Se3 (solid line), its thickness is instead HWOT. An ideal film still exhibits some reflection because we modelled the reflection from the back substrate-air interface.

Fig. 3. Reflectance comparison of each single-layer thin film design. At 1064 nm, an ideal film with nf = 1.21 (dotted) has reflectance = 3.4%, MgF2 with nMgF = 1.38 (dashed line) has reflectance = 5%, and Sb2Se3 (solid line) has reflectance = 6.5%.

## 2.3 Multilayer antireflection design

A two-layer device with QWOT in each layer (Q/Q design) can also achieve a complete antireflection condition. The Fresnel reflection coefficient (r) from Eq. 7 can be expanded to:

r=na-nr2na+nr2,						(11)

r=na-(nf22nr1)na+(nf22nr1),	 					(12)

r=na-(nf22nf12/ns)na+(nf22nf12/ns),	 					(13)

where the film numbering (nf) starts from substrate side and increases toward air (ns/nf1/nf2/na), nr2 is the effective reflectance index of the entire structure [39], and nr1 is the effective reflectance index of only substrate and bottom film. Antireflection condition (r = 0) occurs when:

na=nf22nf12/ns,						(14)

or:

nans=nf22nf12.						(15)

This means that the refractive index of the top film must be smaller than the bottom film (nf2 < nf1). As an example, at 1064 nm if we use the same SiO2 as substrate and Sb2Se3 as bottom film (nf1=3.37), the required refractive index of nf2 is calculated to 2.78. A commonly used material with the closest refractive index is TiO2 with nf2=2.31 [43], so a complete antireflection cannot be achieved. As shown in Fig. 4, when compared to a single-layer design, two-layer design allows for wider materials combinations, has lower reflectivity, and broader operation wavelength. Another way to create a perfect AR condition is to fix the two materials refractive index and vary each layer thickness instead, as described in chapter 5.2 of [39]. However, this method narrows the antireflection bandwidth.

A three-layer design (Q/H/Q) has a HWOT layer placed in the middle. The required refractive index ordering of each layer is ns < nf1 < nf2 and nf2 > nf3 > na. The middle layer (nf2) acts an absentee layer when incident wavelength (λ) is the same as reference wavelength (λ0), but it acts as compensating layer for restoring AR condition for scenarios where λ differs from λ0, a more detailed explanation is provided in chapter 5.4 of [39]. The reflectivity from Eq. 7 is equal to:

r=na-nr3na+nr3=na-(nf32nr2)na+(nf32nr2).						(16)

Because the middle film layer (nf2) is HWOT thick, it behaves as an absentee layer [39, 44]. So nr2 = nr1 and Eq. 16 becomes:

r=na-(nf32nr1)na+(nf32nr1)=na-(nf32nf12/ns)na+(nf32nf12/ns).						(17)

A three-layer antireflection condition occurs when:

nans=nf32nf12.						(18)

The refractive index ratio between top and bottom film is the same as with the two-layer (Q/Q) design, which means a complete AR condition also cannot be achieved. The benefit of adding HWOT middle layer (nf2) is its contribution to a broader operational bandwidth [44]. Its reflection at wavelength farther from λ0, such as at 1400 nm and above, is lower than that of a single or two-layer designs.

Instead of using Sb2Se3 as the bottom film layer (nf1), Sb2Se3 can be moved to the middle layer (nf2), the selection of nf1 and nf3 could then be more practicable. For example, at 1064 nm, the bottom layer could be Si3N4 (nf1 = 2.00 [45]). Using equation 17, the required top layer index is calculated to nf3 = 1.65, Al2O3 has the closest refractive index of 1.62 [43]. This is illustrated in Fig. 4 where the reflectance of the single-layer, two-layer, and three-layer designs, all of which have Sb2Se3 directly on top of the substrate (nf1 = Sb2Se3), are ~6.7%. But when Sb2Se3 is placed in the middle (nf2 is Sb2Se3) reflectance falls to 3.5% and at a broader wavelength, this improvement can be explained by the selection of materials for nf1 and nf3 that are closer to ideal values.

Fig. 4. Reflectance comparison of a single-layer, two-layer, and three-layer antireflection designs. The single-layer design is the same as in Fig. 3. The single-layer, two-layer and three-layer with nf1 = Sb2Se3 designs have around the same reflectance of 6.7% at 1064 nm. The three-layer design with nf2 = Sb2Se3 with HWOT has lowest reflectance at 3.5%, around the same value as the design with an ideal single-layer film in Fig. 2.

## 2.4 Fabry–Pérot cavity design

In all the previous designs, the behaviour after phase transition hasn’t been considered yet. Figure 5 add the calculation for each design in Fig. 4 with same thickness but change the refractive index of amorphous Sb2Se3 (blue) to crystalline Sb2Se3 (orange). The design with the highest reflectance contrast is a single-layer design at 55.0% (Fig. 5a). As for three-layer design with Sb2Se3 in the middle layer, even though it shows the best performance in the amorphous phase, its reflectance contrast is the lowest at only 0.5% (Fig. 5b). This is another requirement for optical limiter, where aside from low reflection, a high enough reflectance contrast after phase transition is necessary.

Fig. 5. Reflectance comparison of the previous designs before (ON mode; blue) and after (OFF mode; orange) phase transition. (a) shows the single and two-layer designs. (b) shows the three-layer designs with Sb2Se3 on the bottom (dash) or middle layer (dotted). A single-layer design shows the highest reflectance contrast when undergoes phase transition. Black vertical lines indicate λ0 = 1064 nm.

A Fabry–Pérot cavity design acts as edges filter with high reflection around the reference wavelength (λ0), but has high transmission beyond the edges. The design can consist of either (H2LH2) or (L2HL2) symmetrical unit cell(s) for high-pass or low-pass design, respectively, where H and L denote material with high and low refractive index contrast, respectively, H and L are QWOT films, and 12 denotes a QWOT2 thick films. Since Fabry–Pérot cavity shows high reflection at λ0, and we design our optical limiters to operate at 1064 nm, λ0 must be changes to a shorter (high-pass) or longer (low-pass) wavelength. A shorter λ0 is preferred since it mean each layer physical thickness will be lower (Eq. 3), so a high-pass (H2LH2) design will be used. The spectral width of high reflection region is determined by the refractive index difference between H and L layers, the larger the difference the wider the spectral width. The sharpness of the spectral edge is directly correlated to the number of unit cells. Figure 6 shows example designs with (H2LH2) unit cell(s), with Sb2Se3 as H and MgF2 as L layer, and λ0 = 750 nm. Figure 6a is the reflectance comparison between different number of unit cells, designs with more cell numbers show a sharper spectral edge. It is interesting to note that design with 8-unit cells (dotted) has a sharper edge than 4-unit cells design (loosely dash), but the reflectance at around 1350 and 1600 nm are higher than 4-unit cells, so a larger number of unit cells doesn’t necessarily give better performance. Figure 6b shows a comparison of amorphous and crystalline Sb2Se3 of 4 unit-cell design; the reflectance in amorphous and crystalline phase are 6.5% and 94.1%, respectively, so the reflectance contrast at 1064 nm is 87.6% which is the highest of any designs shown so far. Another point to note is that the reflection in amorphous phase is around the same as other designs with Sb2Se3 directly on top of the SiO2 substrate.

Fig. 6. Reflectance comparison of Fabry–Pérot cavity (H2LH2) designs with (a) varying number of unit cells and (b) design with 4-unit cells before and after phase transition. Black vertical line indicates λ = 1064 nm, the target operating wavelength of optical limiters. All designs have reference wavelength λ0 = 750 nm.

Another planar thin-film design is the resonant cavity design, which can be used to enhance the optical properties of the middle layer (PCM in this work) [40]. The cavity consists of the PCM layer in the middle and distributed Bragg reflectors on each side of the PCM. The two reflectors function as mirrors that cause light to cycles through the central PCM layer multiple times, this effectively reduced the required thickness of PCM. This benefit is especially useful for PCM with high Ttrans such as Sb2Se3 because it lowers the energy requirement to initiate phase transition, and negates damage caused by partial phase transition due to PCM being too thick [17, 32]. The mirror structure can be described as a form of unit cell (U) composed of high (H) and low (L) refractive index materials with QWOT. The difference between H and L index directly correlated to the enhancement. In this work, we denoted unit cell as U=[H/2 L H/2], where 1/2 indicates a film with half of QWOT or λ/8. For example, a symmetrical cavity with U=1 on each side of the central (C) PCM layer can be written as:

H2 U1 C U1H2, 						(18)

H2H2LH2CH2LH2H2, 					(19)

The limitations of this design is its narrow operation range, and the difficulty in fabrication process.

## 2.5 Antireflection design with absorptive film

In all the previously discussed designs, Sb2Se3 have little to no absorption at the designed 1064-nm wavelength. But its k-index at 532 nm is significant, 1.09 and 2.24 for amorphous and crystalline Sb2Se3, respectively. The effect of k-index absorption can be explained on a single-layer design (Fig.2), an antireflection condition only occurs when both R1 and R2 light have the same amplitude but a phase difference of π radian. If the material has k-index, some of the light travelled through will be absorbed and converted to thermal energy, which mean the amplitude of R1 will reduce. We can visualize this by plotting the effective reflective index (nr) from Eq. 4. as a function of phase thickness (θ) from Eq.5 to create a contour graph [39], the x-axis is the refractive index of the structure, y-axis is its phase, and the starting point is the refractive index of substrate (nsubstrate = nSiO2 = 1.47). To create an antireflection condition, the ending point should come back to the starting point (or for a perfect AR, the ending point should be the incident medium, air). Figure 7 compares a lossless designs (HWOT) with amorphous Sb2Se3 film, which have complex refractive index ña = 3.96 + 1.09i at 532 nm, to an imaginary film with the same n-index but zero k-index (ñimag = 3.96 + 0.00i). The contour graphs are shown in Fig. 7a. with nSiO2 = 1.47 + 0i as the starting point, only when there is no k-index can the contour line return to the starting point.

Fig. 7. Comparison between Sb2Se3 with k-index (solid line) and a lossless Sb2Se3 without k-index (dotted line). (a) Effective reflective index (nr) when θ = π radian (HWOT); only with lossless film can the contour line return to the starting point, an antireflection condition. (b) Even though both designs use the same λ0 = 532 nm, only lossless film reached the lowest reflection at λ0, Sb2Se3 with k-index has the lowest reflection shifted to 594 nm.

In a single-layer design of Fig.2, zero reflection happens when the phases of R1 and R2 is opposite but their amplitudes are the same. If the film has any k-index, such as in the case of Sb2Se3, some of the light will be absorb and R1 will have lower amplitude than R2. This effect is especially magnified in resonant cavity design. One way to visualize this is to plot reflectivity (r) in a contour graph. Figure 4 illustrates the effect material with k-index has on resonant loss. The two designs are optimized for resonant at 1064 nm wavelength, they have U=2 on each side of the central layer. Refractive index of H and L films are the same for both designs, 2.45 and 1.63, respectively. These two designs assume substrate to have the same refractive index as air. The central cavity layer in Fig.5a is equal to C=3.96+0i. For Fig.5b central layer is the same material except it has k-index term, C=3.96+1.09i.

# 3. Methods

## 3.1 Optical limiter design

In this work, we use transfer matrix method (TMM) of Fresnel equation to calculate the transmittance, absorptance, and reflectance of devices. In some simulation works, the substrate index can consider to be equal to air (nsub = nair = 1.0) to simplify the design and allows for a more widely applicable analysis methods, this could be done in reality by applying antireflection coating on the back side of the substrate [40]. But in this work, we choose to use 3-mm thick silica (SiO2) as substrate with refractive index data taken from [46], its refractive index is around 1.47 at both 1064 and 532 nm wavelengths. The H layers are Si [47], TiO2 [43] and Si3N4 [45]. The L layers are Al2O3 [43], SiO2 and MgF2 [42]. All the above mentioned material refractive indices can be found on refractiveindex.info website [48], but since antimony triselenide (Sb2Se3) is a relatively new material in the field of optics, its refractive index couldn’t be found there. We use dataset from [22], as shown in Fig. 1. The refractive index of air is set na = 1.0 across the spectra. The incident angle is 0° and light is transverse electric (TE) polarized for all calculations.

Our optical limiters are designed will either be designed for 1064 or 532 nm wavelengths. For 1064-nm devices, the designs are single-layer, multi-layer, and edge-filter. The goals are to design broadband optical limiter with large transmission contrast (ΔT) between the two modes. Because of the low absorption caused by near-zero k-index in both phases at this wavelength, the devices cannot be self-activated. Since Sb2Se3 have high k-index at 532-nm wavelength, ka = 1.09 and kc = 2.24, we will compare regular design approaches (e.g., single or multi-layer designs) to asymmetrical cavity design. The goal is to showcases different self-activating optical limiter designs and their transmission, absorption, PCM used, and overall device thickness.

## 3.2 Simulation of endurance and optical stability under phase switching cycles

Experimental studies have demonstrated that Sb2Se3 can have phase switching cycles with minimal degradation to its optical contrast up, and maintain a low-loss, reversible modulation in an order of 104 [cite] and 106 cycles [32]. Even so, Sb2Se3 still exhibits slight complex refractive index drift due to structural relaxation and cumulative thermal damage. Accounting for these variations is essential for ensuring long-term reliability and precision in high-endurance photonic applications [32, 33]. To account for this, the complex refractive index (ñ) can  be rewritten from Eq. 1 as:

npN=npN+ikpN	,					(XXX)

where N is the number of phase switching cycle.

The real part of the refractive index (n) is described by an exponential relaxation towards a saturated value such that:

npN=np,∞-np,∞-np,0exp-αpN,				(XXA)

where np,∞ is the asymptotic index after many cycles, np,0 is the refractive index at the first cycle (obtained from ellipsometry or literature data), and αp is the drift coefficient per cycle of phase p [22, 49].

Meanwhile, the imaginary part (k) can be approximated from a linear growth as:

kpN=kp,0(1+βpN),						(XXB)

where kp,0 is the initial loss and βp is the loss growth coefficient. The parameter βp is the relative loss per cycle of phase p [32, 50]. These models from Eq. (XXA) and (XXB) are adopted in this work, they are consistent with experimental trends and with general PCM endurance theory, providing a practical way to assess contrast degradation and threshold drift of PCM-based optical limiters over large cycles [22, 32, 49-51]. A more detailed derivation these endurance models are shown in Supplementary Material.

The endurance of optical limiters can be quantified using the following metrics: 1) transmitting contrast degradation, and 2) insertion loss.

#### Transmitting Contrast Degradation:

Degradation is defined as the reduction in transmission contrast after N cycles, as in:

D(N)=ΔT(N)-ΔT0ΔT0, 					(XX)

where transmission contrast ΔT0 is the contrast of optical device between amorphous (ON) and crystalline (OFF) phases initially (cycle = 0). Transmission contrast (ΔT )can be defined as: (Ta – Tc or Tc – Ta)

ΔTN=TaN- TcN.					(XX)

#### Insertion loss:

The insertion loss of the device at cycle N compares it transmittance to a reference state of cycle 0 [52], such that: Tc(1) or Tc(0)?

ILdBN=10logTc(N)Tc(1).					(XX)

A growing IL(N) indicates increasing loss, typically driven by the linear growth of the imaginary index kp(N) and by detuning of the resonance due to drift of np(N).

# 4. Results

## 4.1 1064-nm optical limiters

Antimony triselenide shows little to no absorption in the infrared spectra, so an ideal design could have 100% transmission in the ON mode and 0% in the OFF mode. The transmission of each mode, transmission contrast, Sb2Se3 thickness, overall device thickness and the number of thin film layers needed for each previously discussed design are show in Table 1. Aside from the single-layer design, only Fabry-Perot designs show transmission contrast (ΔT) higher than 50% with 6 unit-cell design having the largest ΔT.

Table 1. Designs of 1064-nm optical limiter. Transmission is calculated at λ = 1064 nm. The Fabry-Perot cavity designs have λ0 = 750 nm.

| Design | Layout | Number of layers | SbSe used (nm) | Device size (nm) | T (ON) (%) | T (OFF) (%) | ΔT (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Single-layer | SbSe | 1 | 157.9 | 157.9 | 93.5 | 37.2 | 56.3 |
| Two-layer | SbSe/TiO | 2 | 78.9 | 194.1 | 93.3 | 76.9 | 16.4 |
| Three-layer | SbSe/MgF/TiO | 3 | 78.9 | 580.3 | 93.3 | 76.9 | 16.4 |
| Three-layer | SiN/SbSe/AlO | 3 | 157.9 | 455.7 | 96.6 | 83.3 | 13.3 |
| Fabry-Perot | (SbSe2/MgF/SbSe2)1 | 3 | 44.1 | 179.9 | 95.1 | 65.4 | 29.7 |
| Fabry-Perot | (SbSe2/MgF/SbSe2)2 | 5 | 88.1 | 359.8 | 96.6 | 27.6 | 69.0 |
| Fabry-Perot | (SbSe2/MgF/SbSe2)4 | 9 | 176.3 | 719.6 | 93.5 | 2.8 | 90.7 |
| Fabry-Perot | (SbSe2/MgF/SbSe2)5 | 11 | 220.3 | 899.5 | 95.3 | 0.8 | 94.5 |
| Fabry-Perot | (SbSe2/MgF/SbSe2)6 | 13 | 264.4 | 1,079.4 | 96.5 | 0.3 | 96.2 |
| Fabry-Perot | (SbSe2/MgF/SbSe2)8 | 17 | 352.5 | 1,439.3 | 93.6 | 0.0 | 93.6 |

# 5. Discussions

For a 1064-nm optical limiters, a simple QWOT-design already satisfy anti-reflection conditions, it’s also the smallest design. For a broader operating range in the IR spectrum, the XXX design has…

For a self-activating optical limiter at 532 nm, resonance can be restored with asymmetrical designs. Asymmetrical cavity designs required thinner Sb2Se3. Which should prevent partial phase-transition described in [32]. The question then becomes ‘at what threshold of laser intensity will the optical limiter be turned off? If the threshold is low, then the device needs to have more absorptivity in the ON mode. But if the threshold is high, then the absorptivity in the ON mode does not need to be as high. Its absorptivity in the OFF mode is also important; it ideally should be as high as possible since it need to be re-amorphized at an even higher temperature to return the device from OFF to ON mode. Would a volatile-type PCM be more suitable for self-activating optical limiter?

Another metric that we didn’t show here are the tolerance of optical performances at varying incident angles. A high-tolerance devices would allow for broader applications.

Finite Element Method (FEM) [6]

The Fabry-Perot designs have PCM separated into many layers, which could complicated phase switching methods. If we use laser as switching method, the phase transition of each Sb2Se3 layer is not simultaneous, such that the transmission contrast will increase in a gradual sense, this effect can be seen in Sarangan, et al. [4]’s work, their self-activating optical limiter use (H2LH2)4 unit cells design but use GST as PCM instead of Sb2Se3, their experimental result shows that the switching of GST is done layer-by-layer in a sequence determined by the changing optical field distribution and the thermal crosstalk between layers.

Our work still lacks thermal analysis which will determine the laser phase switching schemes for both 532 and 1064 nm design.

# Note

Opt. Commun.

Opt. Laser Technol.

สอบหัวข้อ: Ratchapak Chitaree, Witoon Yindeesuk, Prathan Buranasiri. วันอังคารที่ 9 มิถุนายน ช่วงเช้

Note:

1550:

MgF2:	1.3746		[42]

SiO2: 	1.4443		[46]

Al2O3: 	1.6141		[43]

Si3N4: 	1.9904		[45]

TiO2:	2.2899		[43]

Sb2Se3:	3.2854 (4.0499)	[22]

Si_cry_300k:	3.4795	[53]

Si_amo_20deg: 	3.7771	[47]

1064:

MgF2:	1.3777		[42]

SiO2: 	1.4671		[46]

Al2O3: 	1.6165+0i	[43]

Si3N4: 	1.9966+0i	[45]

TiO2:	2.3097		[43]

Sb2Se3:	3.369674+0i (4.3081+0.009744i)	[22]

Si_cry_300:	3.5552	[53]

Si_amo_20deg: 	3.9017	[47]

532:

MgF2:	1.3842		[42]

SiO2: 	1.4754		[46]

Al2O3: 	1.6311+0i	[43]

Si3N4: 	2.0341+0i	[45]

TiO2:	2.4503		[43]

Sb2Se3:	3.9615+1.093042i (4.7876+2.240748i)	[22]

Si_cry_300:	4.1473+0.039769i	[53]

`	Si_amo_20deg:	4.9143+0.66141i		[47]

# 6. Conclusions

# 7. Acknowledgement

# 8. References

[1]	K. Matuszek, M. Kar, J. M. Pringle, and D. R. MacFarlane, "Phase Change Materials for Renewable Energy Storage at Intermediate Temperatures," Chemical Reviews, vol. 123, no. 1, pp. 491–514, 2023/01/11 2023, doi: 10.1021/acs.chemrev.2c00407.

[2]	R. Matos and N. Pala, "A Review of Phase-Change Materials and Their Potential for Reconfigurable Intelligent Surfaces," Micromachines, vol. 14, no. 6, p. 1259, 2023. [Online]. Available: https://www.mdpi.com/2072-666X/14/6/1259.

[3]	U. Biswas, S. A. Chanu, S. Alam, A. Ashraf, and R. K. Sonkar, "Design of Optical Limiter Using Nonlinear Kerr Effect for the “Far Ultraviolet-C” Band," in 2025 IEEE Photonics Conference (IPC), 9–13 Nov. 2025 2025, pp. 1–2, doi: 10.1109/IPC65510.2025.11281888. [Online]. Available: https://ieeexplore.ieee.org/stampPDF/getPDF.jsp?tp=&arnumber=11281888&ref=

[4]	A. Sarangan, J. Duran, V. Vasilyev, N. Limberopoulos, I. Vitebskiy, and I. Anisimov, "Broadband Reflective Optical Limiter Using GST Phase Change Material," IEEE Photonics Journal, vol. 10, no. 2, pp. 1–9, 2018, doi: 10.1109/jphot.2018.2796448.

[5]	C. Wan et al., "Ultrathin Broadband Reflective Optical Limiter," Laser & Photonics Reviews, vol. 15, no. 6, p. 2100001, 2021, doi: https://doi.org/10.1002/lpor.202100001.

[6]	X. Ling, X. Pang, X. Chen, and Z. Shao, "Broadband mid-infrared optical limiter based on&#x00A0;vanadium dioxide phase transition," J. Opt. Soc. Am. B, vol. 42, no. 9, pp. 2062–2067, 2025/09/01 2025, doi: 10.1364/JOSAB.569492.

[7]	M. Gandolfi et al., "Optical Limiting Thin Multilayer Films Based On Phase Transition In VO2," in 2022 Sixteenth International Congress on Artificial Materials for Novel Wave Phenomena (Metamaterials), 12–17 Sept. 2022 2022, pp. 148–150, doi: 10.1109/Metamaterials54993.2022.9920767. [Online]. Available: https://ieeexplore.ieee.org/stampPDF/getPDF.jsp?tp=&arnumber=9920767&ref=

[8]	A. Tognazzi et al., "Opto-thermal dynamics of thin-film optical limiters based on the VO2 phase transition," Opt. Mater. Express, vol. 13, no. 1, pp. 41–52, 2023/01/01 2023, doi: 10.1364/OME.472347.

[9]	A. Donval, Y. Ofir, D. Nevo, and M. Oron, "Reflective Optical Limiter," US Patent US 2014/0233085 A1 Patent Appl. US 201214343922 A, 2014/08/21, 2014. [Online]. Available: https://lens.org/107-268-237-474-798

[10]	A. N. H. Lam Tai, "OPTICAL LIMITERS FOR FACILITATING APERTURE PROTECTION," US Patent US 2019/0094430 A1 Patent Appl. US 201715716364 A, 2019/03/28, 2019. [Online]. Available: https://lens.org/168-829-457-144-045

[11]	W. Jia, R. Menon, and B. Sensale-Rodriguez, "Unique prospects of phase change material Sb2Se3 for ultra-compact reconfigurable nanophotonic devices," Opt. Mater. Express, vol. 11, no. 9, pp. 3007–3014, 2021/09/01 2021, doi: 10.1364/OME.435979.

[12]	P. Xu, J. Zheng, J. K. Doylend, and A. Majumdar, "Low-Loss and Broadband Nonvolatile Phase-Change Directional Coupler Switches," ACS Photonics, vol. 6, no. 2, pp. 553–557, 2019/02/20 2019, doi: 10.1021/acsphotonics.8b01628.

[13]	Y. Zhang et al., "Broadband transparent optical phase change materials for high-performance nonvolatile photonics," Nature Communications, vol. 10, no. 1, p. 4279, 2019/09/30 2019, doi: 10.1038/s41467-019-12196-4.

[14]	H. Li, D. Zeng, Y. Huang, Q. Huang, and X. Zhang, "Ultra-compact, ultra-low-loss and broadband 2 x 2 nonvolatile optical switch based on Sb(2)Se(3) phase change material," Opt Express, vol. 32, no. 20, pp. 35287–35297, Sep 23 2024, doi: 10.1364/OE.534645.

[15]	D. d. Ceglia, M. Grande, A. Vincenti, C. Baratto, and C. d. Angelis, "Tunable Filters for Visible Light Based on Resonant VO2 Planar Thin Films," in 2020 22nd International Conference on Transparent Optical Networks (ICTON), 19–23 July 2020 2020, pp. 1–4, doi: 10.1109/ICTON51198.2020.9203244.

[16]	R. Heenkenda, K. Hirakawa, and A. Sarangan, "Tunable optical filter using phase change materials for smart IR night vision applications," Opt. Express, vol. 29, no. 21, pp. 33795–33803, 2021/10/11 2021, doi: 10.1364/OE.440299.

[17]	Y.-S. Huang et al., "Tunable structural transmissive color in fano-resonant optical coatings employing phase-change materials," Materials Today Advances, vol. 18, p. 100364, 2023/06/01/ 2023, doi: https://doi.org/10.1016/j.mtadv.2023.100364.

[18]	C. Wan et al., "Limiting Optical Diodes Enabled by the Phase Transition of Vanadium Dioxide," ACS Photonics, vol. 5, no. 7, pp. 2688–2692, 2018/07/18 2018, doi: 10.1021/acsphotonics.8b00313.

[19]	H. Kocer et al., "Intensity tunable infrared broadband absorbers based on VO2 phase transition using planar layered thin films," Scientific Reports, vol. 5, no. 1, p. 13384, 2015/08/21 2015, doi: 10.1038/srep13384.

[20]	X. Tian and Z.-Y. Li, "An Optically-Triggered Switchable Mid-Infrared Perfect Absorber Based on Phase-Change Material of Vanadium Dioxide," Plasmonics, vol. 13, no. 4, pp. 1393–1402, 2018/08/01 2018, doi: 10.1007/s11468-017-0643-9.

[21]	C. Liu et al., "Tunable nonlinear optical absorption in amorphous and crystalline Sb2Se3 thin films," Journal of Alloys and Compounds, vol. 791, pp. 753–760, 2019/06/30/ 2019, doi: 10.1016/j.jallcom.2019.03.295.

[22]	M. Delaney, I. Zeimpekis, D. Lawson, D. W. Hewak, and O. L. Muskens, "A New Family of Ultralow Loss Reversible Phase‐Change Materials for Photonic Integrated Circuits: Sb2S3 and Sb2Se3," Advanced Functional Materials, vol. 30, no. 36, 2020, doi: 10.1002/adfm.202002447.

[23]	Z. Gong et al., "Phase change materials in photonic devices," Journal of Applied Physics, vol. 129, no. 3, 2021, doi: 10.1063/5.0027868.

[24]	A. A. Burtsev et al., "Physical properties’ temperature dynamics of GeTe, Ge2Sb2Te5 and Ge2Sb2Se4Te1 phase change materials," Materials Science in Semiconductor Processing, vol. 150, p. 106907, 2022/11/01/ 2022, doi: https://doi.org/10.1016/j.mssp.2022.106907.

[25]	P. Guo, Z. Biegler, T. Back, and A. Sarangan, "Vanadium dioxide phase change thin films produced by thermal oxidation of metallic vanadium," Thin Solid Films, vol. 707, p. 138117, 2020/08/01/ 2020, doi: https://doi.org/10.1016/j.tsf.2020.138117.

[26]	M. E. A. Warwick and R. Binions, "Advances in thermochromic vanadium dioxide films," Journal of Materials Chemistry A, 10.1039/C3TA14124A vol. 2, no. 10, pp. 3275–3292, 2014, doi: 10.1039/C3TA14124A.

[27]	Y. Cui et al., "Thermochromic VO2 for Energy-Efficient Smart Windows," Joule, vol. 2, no. 9, pp. 1707–1746, 2018/09/19/ 2018, doi: https://doi.org/10.1016/j.joule.2018.06.018.

[28]	J. Sang et al., "Smart Windows with a VO2 Thin Film as a Conductive Layer for Efficient and Independent Dual-Band Modulation," ACS Applied Electronic Materials, vol. 3, no. 11, pp. 4882–4890, 2021/11/23 2021, doi: 10.1021/acsaelm.1c00728.

[29]	N. Murillo-Quirós, V. Vega-Garita, A. Carmona-Calvo, E. A. Rojas-González, R. Starbird-Perez, and E. Avendaño-Soto, "Toward Thermochromic VO2 Nanoparticles Polymer Films Based Smart Windows Designed for Tropical Climates," Polymers, vol. 14, no. 19, p. 4250, 2022. [Online]. Available: https://www.mdpi.com/2073-4360/14/19/4250.

[30]	X. Chen, J. Lin, and K. Wang, "A Review of Integrated Photonic Devices Using Sb2Se3," Advanced Physics Research, vol. 4, no. 1, p. 2400080, 2024, doi: 10.1002/apxr.202400080.

[31]	C. Chen et al., "Optical properties of amorphous and polycrystalline Sb2Se3 thin films prepared by thermal evaporation," Applied Physics Letters, vol. 107, no. 4, 2015, doi: 10.1063/1.4927741.

[32]	D. Lawson, S. Blundell, M. Ebert, O. L. Muskens, and I. Zeimpekis, "Optical switching beyond a million cycles of low-loss phase change material Sb2Se3," Opt. Mater. Express, vol. 14, no. 1, 2023, doi: 10.1364/ome.509434.

[33]	M. S. Alam et al., "Fast Cycling Speed with Multimillion Cycling Endurance of Ultra-Low Loss Phase Change Material (Sb2Se3) by Engineered Laser Pulse Irradiation," Advanced Functional Materials, vol. 34, no. 14, p. 2310306, 2024, doi: https://doi.org/10.1002/adfm.202310306.

[34]	J. Faneca et al., "Towards low loss non-volatile phase change materials in mid index waveguides," Neuromorphic Computing and Engineering, vol. 1, no. 1, p. 014004, 2021/08/23 2021, doi: 10.1088/2634-4386/ac156e.

[35]	S. Blundell et al., "Ultracompact Programmable Silicon Photonics Using Layers of Low-Loss Phase-Change Material Sb2Se3 of Increasing Thickness," ACS Photonics, vol. 12, no. 3, pp. 1382–1391, 2025/03/19 2025, doi: 10.1021/acsphotonics.4c01789.

[36]	J. H. Vella et al., "Experimental Realization of a Reflective Optical Limiter," Physical Review Applied, vol. 5, no. 6, p. 064010, 06/20/ 2016, doi: 10.1103/PhysRevApplied.5.064010.

[37]	C. Baratto et al., "Optical Limiting Sensor Based on Multilayer Optimization of Ag/VO2 Phase Change Material," IEEE Sensors Letters, vol. 7, no. 9, pp. 1–3, 2023, doi: 10.1109/LSENS.2023.3300801.

[38]	L. Shah, S. Cannon Roger, and A. Drummer Mark, "LIDAR RECEIVER OPTICAL LIMITER," US Patent US 2025/0172672 A1 Patent Appl. US 202418960941 A, 2025/05/29, 2025. [Online]. Available: https://lens.org/118-293-389-504-62X

[39]	A. Sarangan, Optical Thin Film Design, 1st Edition ed. Boca Raton: CRC Press, 2020.

[40]	A. Sarangan, "Design of resonant cavity thin film structures with complex active layers," J. Opt. Soc. Am. B, vol. 37, no. 11, pp. 3461–3468, 2020/11/01 2020, doi: 10.1364/JOSAB.404894.

[41]	L. Gao, F. Lemarchand, and M. Lequime, "Exploitation of multiple incidences spectrometric measurements for thin film reverse engineering," Opt. Express, vol. 20, no. 14, pp. 15734–15751, 2012/07/02 2012, doi: 10.1364/OE.20.015734.

[42]	D. Franta, D. Nečas, A. Giglia, P. Franta, and I. Ohlídal, "Universal dispersion model for characterization of optical thin films over wide spectral range: Application to magnesium fluoride," Applied Surface Science, vol. 421, pp. 424–429, 2017/11/01/ 2017, doi: https://doi.org/10.1016/j.apsusc.2016.09.149.

[43]	S. V. Zhukovsky et al., "Experimental Demonstration of Effective Medium Approximation Breakdown in Deeply Subwavelength All-Dielectric Multilayers," Physical Review Letters, vol. 115, no. 17, p. 177402, 10/23/ 2015, doi: 10.1103/PhysRevLett.115.177402.

[44]	Y. Li et al., "Preparation of mechanically stable triple-layer interference broadband antireflective coatings with self-cleaning property by sol–gel technique," RSC Advances, 10.1039/C7RA00844A vol. 7, no. 24, pp. 14660–14668, 2017, doi: 10.1039/C7RA00844A.

[45]	L. Y. Beliaev, E. Shkondin, A. V. Lavrinenko, and O. Takayama, "Optical, structural and composition properties of silicon nitride films deposited by reactive radio-frequency sputtering, low pressure and plasma-enhanced chemical vapor deposition," Thin Solid Films, vol. 763, p. 139568, 2022/12/01/ 2022, doi: https://doi.org/10.1016/j.tsf.2022.139568.

[46]	D. Franta, D. Nečas, I. Ohlídal, and A. Giglia, Optical characterization of SiO2 thin films using universal dispersion model over wide spectral range (SPIE Photonics Europe). SPIE, 2016.

[47]	O. C. Karaman, G. N. Naidu, A. R. Bowman, E. N. Dayi, and G. Tagliabue, "Decoupling Optical and Thermal Dynamics in Dielectric Metasurfaces for Self-Encoded Photonic Control," Laser & Photonics Reviews, vol. 19, no. 24, p. e01014, 2025, doi: https://doi.org/10.1002/lpor.202501014.

[48]	M. N. Polyanskiy, "Refractiveindex.info database of optical constants," Scientific Data, vol. 11, no. 1, p. 94, 2024/01/18 2024, doi: 10.1038/s41597-023-02898-2.

[49]	L. Martin-Monier et al., "Endurance of chalcogenide optical phase change materials: a review," Opt. Mater. Express, vol. 12, no. 6, pp. 2145–2167, 2022/06/01 2022, doi: 10.1364/OME.456428.

[50]	Y. Zhang et al., "Myths and truths about optical phase change materials: A perspective," Applied Physics Letters, vol. 118, no. 21, 2021, doi: 10.1063/5.0054114.

[51]	S. Kim, G. W. Burr, W. Kim, and S.-W. Nam, "Phase-change memory cycling endurance," MRS Bulletin, vol. 44, pp. 710–714, September 01, 2019 2019, doi: 10.1557/mrs.2019.205.

[52]	R. Paschotta, Encyclopedia of Laser Physics and Technology. Wiley, 2008.

[53]	D. Franta, P. Franta, J. Vohánka, M. Čermák, and I. Ohlídal, "Determination of thicknesses and temperatures of crystalline silicon wafers from optical measurements in the far infrared region," Journal of Applied Physics, vol. 123, no. 18, 2018, doi: 10.1063/1.5026195.