## Slide 1: Ideas
27/11/2025

## Slide 2: Refractive index @1550nm Sb2Se3 vs VO2
Sb2Se3 (Ttransition = 186 °C)
Dataset for A new family of ultra-low loss reversible phase change materials for photonic integrated circuits: Sb2S3 and Sb2Se3
Amorphous: 3.2854 + 0.0000j
Crystalline: 4.0499 + 0.0002j
VO2 (25/100 °C; Ttrans = 68 °C (volatile))
Thermochromic VO2-based smart radiator devices with ultralow refractive index cavities for increased performance
Amorphous: 3.1462 + 0.3388j
Metallic: 1.9277 + 2.9058j

## Slide 4: Refractive index @1550nm Sb2Se3 vs GST
GST (Ttrans = 150 °C, Tamorphization = 600 °C)
Dataset for A new family of ultra-low loss reversible phase change materials for photonic integrated circuits: Sb2S3 and Sb2Se3
Amorphous: 3.2854 + 0.0000j
Crystalline: 4.0499 + 0.0002j
Amorphous: 4.3534 + 0.0608j
Crystalline : 7.9132 + 1.0331j
Sb2Se3 (Ttransition = 186 °C)
Dataset for A new family of ultra-low loss reversible phase change materials for photonic integrated circuits: Sb2S3 and Sb2Se3

## Slide 6: Sb2Se3 pros
Low absorption at C-band (no ref need?)
Large Δn b/w phase (ref?)
High switching endurance 107 cycles (Optical switching beyond a million cycles of low-loss phase change material Sb2Se3)
Crystalline temperature is relatively low (186 °C) (Optical switching beyond a million cycles…)
  In this paper, annealed @200°C for 5 mins.
  Will remain stable at telecommunication usage.
  Can’t find amorphization temp anywhere.
  For comparison, Tcrystallization: GST =180, Sb2S3 =270, GSST = 300+ °C

## Slide 7: Sb2Se3 as optical limiter
  ? Might be suitable for usage in short wl, e.g. shorter than 400 nm.
  Small absorption coefficient (k) in both phase. @ 1550 nm

## Slide 8: Why 532 and 1064 optical limiter?
    Standard wl for Nd:YAG (Neodymium-doped yttrium aluminium garnet) laser (2nd harmonic = 532 nm).
      Find citation(?)

## Slide 9: Refractive index, non-linear effect vs phase transition.
Kerr effect: Intensity dependent
Change due to phase transition: amorphous -> crystalline
“We show that it is possible to shift the transition edge of the filter by several hundred nanometers by utilizing the huge changes in the refractive index of GST. This shift is orders of magnitude larger than that achievable with nonlinear refraction… “ - Broadband Reflective Optical Limiter Using GST Phase Change Material
> Non-linear term should be negligible when compared to index changes due to phase transition.

## Slide 10
  Both device types don’t require Reflection
    Increase Transmission and Absorption
k=2π/λ
(2)
Antireflection (AR)
2 Theory
(3.1)
(3.2)
(3.3)
Quarter-Wave Optical Thickness (QWOT)
nA < nF < nS
8
Bachelor’s pptx

## Slide 11: Results

## Slide 12: 1064 nm Optical limiter
  Refractive index of SbSe:
  Amo = 3.370 + 0.000000j
  Cry = 4.308 + 0.009744j

## Slide 13
  Resonant in amorphous phase

## Slide 14
(1)

## Slide 15
(2)

## Slide 16
  Resonant in crystalline phase

## Slide 17
(1)

## Slide 18
(1)

## Slide 19: 532 nm Optical limiter
  Refractive index of SbSe:
  Amo = 3.962 + 1.093042j
  Cry = 4.788 + 2.240748j

## Slide 20
  Resonant in crystalline phase

## Slide 21
(1)

## Slide 22
(2)

## Slide 23: 600 nm Optical limiter
  Refractive index of SbSe:
  Amo = 3.962 + 1.093042j
  Cry = 4.788 + 2.240748j

## Slide 24: 1064 nm Optical limiter
SiO2 = 3 mm
SbSe = HWOT = 157.9 nm
SiO2 = 3 mm
SbSe = QWOT/2 = 24.75 nm
MgF2 = QWOT = 135.8 nm
SbSe = QWOT/2 = 24.75 nm
1 unit-cell
Single-layer
Edge-filter (N=1)
SiO2 = 3 mm
SbSe = QWOT/2 = 24.75 nm
MgF = QWOT = 135.8 nm
SbSe = QWOT/2 = 24.75 nm
2 unit-cells
Edge-filter (N=2)
SbSe = QWOT/2 = 24.75 nm
MgF = QWOT = 135.8 nm
SbSe = QWOT/2 = 24.75 nm
SiO2 = 3 mm
SbSe = QWOT = 78.9 nm
Two-layer
TiO2 = QWOT = 115.2 nm
Reference wavelength = 1064 nm
Reference wavelength = 750 nm

## Slide 25
SiO2 = 3 mm
SbSe = HWOT = 67.2 nm
SiO2 = 3 mm
TiO2 = QWOT/2 = 27.14 nm
MgF = QWOT = 96.08 nm
TiO2 = QWOT/2 = 27.14 nm
1 unit-cell
Single-layer
Fabry-Perot
N=1(MgF/SbSe) M=0
H = TiO2, L = MgF2
SiO2 = 3 mm
1 unit-cells
532 nm Optical limiter
Reference wavelength = 532 nm
SbSe = 6.6 nm
MgF = 51.4 nm
TiO2 = QWOT/2 = 27.14 nm
MgF = QWOT = 96.08 nm
TiO2 = QWOT/2 = 27.14 nm
TiO2 = QWOT/2 = 27.14 nm
TiO2 = QWOT/2 = 27.14 nm
TiO2 = QWOT/2 = 27.14 nm
SbSe = 7.1 nm
TiO2 = 34.6 nm
SbSe = 7.1 nm
TiO2 = QWOT/2 = 27.14 nm
SiO2 = 3 mm
Single-layer
(non QWOT)
SbSe = 22.6 nm
TiO2 = 56.6 nm
Fabry-Perot
N=1(SbSe/TiO/SbSe) M=0
H = TiO2, L = MgF2

## Slide 26: 1064 nm Optical limiter
Endurance simulation
Single-layer design (HWOT)
Two-layer design (QWOT)
Edge-filter design (N=3)
*ถ้ามีเวลา Edge-filter design (N=1, 5, 8)
532 nm Optical limiter
Endurance simulation
Single-layer
Two-layer (non QWOT)
Fabry-Perot: N1 (MgF/SbSe) M0

## Slide 27
T(amo) = 93.8%
T(cry) = 0.9%
9-layer edge filter

## Slide 28
T(amo) = 93.6%
T(cry) = 0.21%
11-layer edge filter