Design and Simulation of Sb2Se3-Based Symmetric and Asymmetric Resonant Optical Limiters Using Transfer-Matrix Method

Design and Simulation of Sb2Se3-Based Resonant Optical Limiters Using Transfer-Matrix Method

Prathan Buranasiri1, Chettanat Padungatthakij1, Suebtarkul Suchat2, Surawut Wicharn 3*

1Department of Physics, School of Science, King Mongkut’s Institute of Technology Ladkrabang, 1 Chalongkrung Rd. Ladkrabang, Bangkok, Thailand 10520;

2 Department of Physics, Faculty of Science and Technology, Phranakhon Rajabhat University, 9 Chaengwattana Rd., Bang Khen, Bangkok, Thailand 10220;

3Department of Physics, Faculty of Science, Srinakharinwirot University, 114 Sukhumvit 23 Watthana, Bangkok, Thailand 10110

Email: surawutw@g.swu.ac.th

*Corresponding author

Abstract

We propose a novel optical limiter design utilizing asymmetric resonant cavities composed of Sb2Se3 phase change material (PCM) thin film layer. This design addresses critical limitations of conventional optical limiting devices by exploiting the exceptional properties of Sb2Se3, including ultra-low optical losses, large refractive index contrast, and superior switching endurance exceeding 10⁶ cycles. The Fabry-Perot cavity architecture incorporates optimized Sb2Se3 layer with thicknesses ranging from 20-100 nm, strategically positioned between multilayered thin film structure of distributed Bragg reflectors (DBRs) to achieve directional light transmission and controlled threshold switching. The device operates through thermally induced phase transitions in Sb2Se3, transitioning between amorphous and crystalline states. This approach represents a significant advancement in photonic devices, offering superior performance metrics compared to traditional optical limiters while maintaining excellent reversibility and endurance. The design has potential applications in optical communication systems, laser protection devices, and reconfigurable photonic circuits, contributing to the development of next-generation smart optical components.

Keywords: Optical limiter; Asymmetric resonant cavity; Phase change material; Tunable transmission

#### 1. Introduction

Phase change materials (PCMs) have a different meaning depending on the topics [1]. When discussing energy storage, the term would refer to materials that store and release thermal energy by changing their state of matter, (i.e. latent heat). The transition between phase is between solid and liquid [2]. However, in photonics and electronics, PCMs refer to solid-state material that change its crystalline structure when sufficient energy is applied, and the temperature rises above transition temperature (Ttrans). The transformation of crystalline structure leads to a change in optical properties, such as the refractive index (n) [3]. The change in refractive index associated with nonlinear behavior due to phase transition orders of magnitude larger than changes induced by an applied electric field or light intensity (Kerr effect) [4]. The large contrast makes PCMs ideal for photonic applications that behave similarly to a switch or a filter. Such as a tunable optical filter [5, 6], broadband absorber [7, 8], gas sensor [9], optical limiter [4, 10-12], optical switch [13, 14], or an optical diode [15].

PCM can be classified by their post phase-transition behavior. A volatile PCM reverts to their original phase if the temperature drops below Ttrans but non-volatile PCM will remain in the transitioned phase. To return a non-volatile PCM to its pre-transitioned phase, a higher melting temperature needs to be reached and then rapidly quenched. A commonly studied PCMs in photonics thin film are Ge2Sb2Te5 (GST), Ge-Sb-Se-Te (GSST), and Vanadium dioxide (VO2).

A commonly studied non-volatile PCM is GST. It exhibits large refractive index contrast between the amorphous and crystalline phase [16]. It has relatively low crystallization temperatures at ~180°C. Thin film devices made from GST can be thin due to a high refractive index contrast. A thin device with low transition temperature allows for an easy phase switching. But GST devices suffer from inefficiency due to a large extinction coefficient (k), which results in high optical loss. GSST is a derivative of GST that substitutes some of the antimony to selenium. GSST has a lower optical absorption than GST but has a lower refractive index contrast. It also has a higher crystallization temperature, at around 265 °C, than GST [17].

In the past 10 years, VO2 has gathered attention as a volatile phase change material with the closest metal-to-insulation transition (MIT) temperature to room temperature among other common PCMs, at 68 °C [6, 8, 18, 19]. It also has a relatively high refractive index contrast between the two phases in the infrared spectrum. Its drawbacks are a high extinction coefficient, and thermal hysteresis [20]. Even so, its low transition temperature and high refractive index contrast make it an attractive real-world design such as energy-saving thermochromic window coatings that help with room cooling by automatically blocking transmission when heated by strong sunlight during the summer but allows high transmittance in the winter to help with indoor heating [19, 21, 22].

Antimony triselenide (Sb2Se3) was initially used in solar energy applications [23] but is an emerging non-volatile material in the field of photonic [24]. Unlike GST or GSST, it has almost zero extinction coefficients in the infrared spectrum for both amorphous and crystalline phases [14, 25], has a relatively stable refractive index contrast from the visible through infrared spectrum [16]. Its crystallization temperature is around 186 °C, comparable to GST [14]. And it also has been experimentally shown to have high phase switching endurance of 4,000 cycles [16], or with an optimized laser-induced crystallization and re-amorphization process, can be on the order of 106 cycles [14]. These properties make Sb2Se3 popular as a low-loss, reconfigurable photonic devices to be used in an optical waveguide [16, 17, 26-28]. But Sb2Se3 usage as an optical limiter has been mostly unexplored.

An optical limiter is a photonic device that allows light transmission in the normal ‘on’ mode. But it will block transmission by absorption and/or reflection, when switched to ‘off mode. The devices can be designed to operate in single [15, 29, 30] or broad wavelengths [4, 6, 11, 12, 15]. Optical limiter can be switched by self-heating from the high-intensity light of designed wavelength [11, 15, 30, 31] or it can also be manually switched by high-intensity light outside the designed operating wavelength [14]. The latter case allows for more efficient devices, since they can have lower absorption at the operating wavelength. Applications include a filter for sensor/eyes protector [11, 31], or integrated photonic circuits. Ideally, an optical limiter needs to have high transmission contrast between in the on and off mode. The contrast can either be defined as the relative or the ratio between both phases. An ideal optical limiter also should not have high absorption in the on mode, which affects the device efficiency. A resonant cavity distributed Bragg reflector structure with antireflection design provides a solution to both requirements [32]. At resonance wavelength, constructive interference will maximize the transmission of the device. And when PCM switches to off mode, the resulting refractive index contrast will also be enhanced due to the cavity design. The resonant enhancement also means that the central PCM layer can be thinner than PCM in a standalone antireflection design. This benefit is more significant to a non-volatile PCM which has higher transition temperature. And since the use of thinner PCM layer results in a lower energy requirement for the crystallization or re-amorphization process. Another benefit of thinner PCM is the dampening of the stress due to the contraction and expansion of the crystallization and re-amorphization process, enhance the endurance, and help with the thickness limit of thin film design [14, 33].

Since the photonic applications of Sb2Se3 are largely unexplored [24], we decided to investigate Sb2Se3-based thin-film optical limiters. We chose to simulate multilayer approach (thin-film stacks) rather than a metasurfaces design since it’s more feasible to fabricates [31] while still provide the necessary resonance for a cavity design. To demonstrate the benefits and limitations of this design approach, we design the limiters for two distinct wavelengths: 532 and 1,064 nm, which has high and low extinction coefficient, respectively [16]. Moreover, the optimal designed optical limiters for both wavelengths are characterized by their performance stability under million optical cycling conditions. Then, calculated results of the endurance metrics for our samples proof that the Sb2Se3 based resonant cavity structure has a great potential to be used as optical limiters in optical wavelength.

#### 2. Related theories

### 2.1 Sb2Se3 phase change material

Antimony Selenide (Sb₂Se₃) is an orthorhombic chalcogenide characterized by quasi-one-dimensional ribbons. While its amorphous state consists of a disordered network of distorted motifs, crystallization restores long-range order along the ribbon direction. This thermally driven transition triggered by nanosecond to microsecond optical or electrical pulses, mimics traditional phase-change materials but offers significantly lower optical losses [14, 16]. Sb₂Se₃ offers non-volatile phase switching, maintaining its state at room temperature without power. This reversible process supports high endurance, with optical switching reaching 10⁶ - 10⁷ cycles. For optical limiting, the material enables repeatable toggling between high and low transmission states, provided local heating stays below the melting or ablation thresholds [36-37]. Sb₂Se₃ belongs to the family of ultra‑low‑loss optical phase‑change materials, together with Sb₂S₃, designed specifically for photonic applications. In the visible and near‑infrared spectral range, Sb₂Se₃ shows [16, 37]:

- A relatively large real refractive index n(λ) in both phases (typically n ≈ 2.5 − 3.0 in the amorphous state and higher in the crystalline state, depending on wavelength).

- A very small extinction coefficient k(λ) over a broad wavelength range, particularly in the red and near‑infrared where k approaches zero, indicating negligible absorption.

2.1.1 Optical properties of Sb₂Se₃

Sb₂Se₃ has a bandgap in the visible regime, which leads to appreciable absorption in the blue/UV but much lower loss in the green, red, and near‑IR bands where many photonic applications operate. The large contrast Δn = na - nc between crystalline (nc) and amorphous (na) states, combined with the low k in both phases, gives a high phase‑shift‑per‑loss figure of merit compared to traditional PCMs such as Ge₂Sb₂Te₅ [16, 37-38]. The complex refractive index of Sb₂Se₃ is written as:

, 				     (1)

where p indicates amorphous (a) or crystalline (c) phase. Dispersive models such as Tauc–Lorentz or multi‑oscillator fits are often used to represent the measured np(λ) and kp(λ) over the spectral range of interest. Here the dispersion spectrum for real and imaginary parts of complex refractive index according to Eq. (1) are represented in figure 1.

| (a) | (b) |
| --- | --- |

Figure 1. Dispersion spectrum of Sb₂Se₃ at (a) amorphous and (b) crystalline phases.

Figure 1 shows the complex refractive index of Sb₂Se₃ in amorphous and crystalline phases over 200–1700 nm. The blue solid curves correspond to the real part n(λ), and the red dashed curves to the imaginary part k(λ). For the amorphous phase as shown in figure X1a, n increases from about 1.3 at 200 nm to a maximum of around 4.0 near 600 nm, then gradually decreases and saturates around 3.2 above 1200 nm, indicating strong dispersion near the band edge and weaker dispersion in the near‑infrared. The imaginary part peaks around 300 - 350 nm with k ≈ 2 and falls rapidly towards almost zero beyond ~800 nm, so amorphous Sb₂Se₃ is strongly absorbing only in the blue/UV but becomes effectively transparent in the red and near‑IR [16, 37]. For the crystalline phase, the real index is higher across the spectrum, reaching around 5.1 near 600 - 650 nm and decreasing smoothly to around 4.0 in the near‑infrared, giving a substantial phase contrast Δn = nc - na, especially at visible and telecom wavelengths. The imaginary part again peaks in the near‑UV and rapidly approaches zero above ~900 nm, showing that both phases are almost lossless in the near‑infrared region [16].

Compared to conventional PCMs such as VO₂ or Ge₂Sb₂Te₅ (GST), Sb₂Se₃ therefore offers several advantages for operation at visible and near‑infrared wavelengths. In the visible range, Sb₂Se₃ maintains a high real index while exhibiting a significantly lower extinction coefficient than GST, which enables phase modulation with much smaller insertion loss in resonant cavities and waveguides. This is essential for optical limiters that must remain highly transparent for low‑intensity green and red signals but provide strong modulation at high intensity. In the near‑infrared, Sb₂Se₃ becomes almost lossless (k ≈ 0) while preserving a large index contrast between amorphous and crystalline phases, allowing strong phase modulation with minimal absorption and supporting high‑Q cavities and long waveguide sections without excessive loss. These spectral characteristics make Sb₂Se₃ an excellent candidate for broadband optical limiting across visible and near‑infrared bands through appropriate design of cavity thickness and DBR dispersion.

2.1.2 Endurance and stability considerations under optical cycling

Previously, experimental studies demonstrated that Sb₂Se₃ can continue extensive switching cycles with minimal degradation in optical contrast. Both waveguide and thin-film architecture have successfully sustained 104 to 106 cycles while maintaining low-loss, reversible modulation. Despite this robustness, Sb₂Se₃ exhibits slight variations in optical performance over time. Structural relaxation and cumulative thermal damage can induce a subtle drift in the real and imaginary components of the refractive index. Consequently, accounting for these variations in the complex refractive index is essential for ensuring long-term reliability and precision in high-endurance photonic applications [14, 36]. The complex refractive index of Sb₂Se₃ for empirical endurance modeling can be written as:

, 				(2)

where p represents a: amorphous phase and c: crystalline phase, and Ncyc is the optical cycle number. The real part of the refractive index is described by an exponential relaxation towards a saturated value as:

, 				   (3)

where np,0 is the initial refractive index at the first cycle (obtained from ellipsometry or literature data), np,∞ is the asymptotic index after very many cycles, and αp is a drift coefficient (per cycle) for phase p [16, 41]. Meanwhile, the imaginary part by an approximately linear growth as:

, 			                  (4)

or

, 				        (5)

where kp,0 is the initial loss and βp (or γp) is the loss growth coefficient [14, 40]. The parameter βp measures the relative increase of loss per cycle. These models as Eq. (3) and (5) are adopted in this work, but they are consistent with experimental trends and with general PCM endurance theory, providing a practical way to assess contrast degradation and threshold drift of Sb₂Se₃ based optical limiters over many cycles [14, 16, 40-42]. The details of derivation of empirical endurance models of Sb₂Se₃ film are shown in Appendix A.

#### 2.2 Designing of resonant cavity structure and transfer-matrix method

#### 2.2.1 Multilayer antireflection thin film design

The simplest thin film device consists of a single subwavelength-thick film deposited on a substrate. By selecting film with an appropriate refractive index (n) and physical thickness (t) one can design a device that is either highly reflective or has antireflective. Since all the devices discussed in the introduction prioritize transmission or absorption and do not employ reflection for any operation, minimizing their reflectivity is beneficial. In this work, we will make our devices a perfect antireflection (AR) design. A single-layer AR design has 2 interfaces for reflection: the first interface is at the top of the thin film before light enters the film layer (air-film), the second interface is when light reflects at the substrate (film-substrate). Antireflection is archived when light from the second interface travelled π radian out of phase.

Since light travelled through the film layer twice, before and after reflected at the second interface, the film needs to be π/2 phases thick. This can also be described as an optical thickness of quarter-wave optical thick (QWOT). Optical thickness OT is defined as:

,					   (6a)

,						 (6b)

where n is the refractive index, and t is the physical thickness. For example, an AR design for 1,000-nm light needs to have thin film with physical thickness  nm.

Another way to find film thickness for a multilayer AR design is to consider the reflectivity (r). First, we consider only the first reflection interface:

,					        (7)

where na is the refractive index of air, and nf is the refractive index of the film.

Next, if we considered reflectivity of both interfaces, nf can be substituted by effective reflectance index (nr), which can be thought of as the combined index of the all the film layers and substrate. A more detailed explanation can be found in Chapter 3 of [34].

,			             (8)

where θ is phase thickness and is related to the angular wave number (k0) by

, .					   (9)

For perfect antireflection, nr from Eq. (8) must be equal to na so that r will be zero. When the phase thickness is in a multiple of π/2, the exponent terms in Eq. (8) can be simplified to an integer of N as below:

, .				            (10)

Using Euler’s identity, and if N is odd number, θ will be equal to π. Eq. (10) then become

.					    (11)

By substituting Eq. (11) to Eq. (8), nr will be simplified to

,

,

.					   (12)

The physical thickness (t) of the film can be computed by substituting Eq. (10) to Eq. (9) and is also equal to QWOT.

For two-layer devices, the reflectivity condition from Eq. (12) can be expanded in a similar manner to TMM. For example, with a two-layer films on a substrate the reflectivity will be equal to

,

,

.					(13)

To achieve r = 0, the following ratio must be satisfied:

,						  (14)

or

.					     (15)

But this has a limitation of selecting materials with correct ratio between film and substrate index. Which might not be possible due to the limitation of available materials fabrication capability. To help visualize this, a contour graph (admittance locus) can be used. It represents the relationship between the effective reflective index (nr) and the phase thickness (θ). The contour line starts at the index of substrate and ends at the index of air for an AR design. The film phase thickness represents the contour line length, and the refractive index represents the line radius. The imaginary index in the Y-axis represents the phase of the reflection [34].

For multilayer designs, a contour diagram visualizes how each film affects nr. Figure 2 provides an example of a device designed for 550-nm light with ns = 1.5, nf1 = 1.7, and nf2 = 1.4. Both nf1 and nf2 are QWOT.

Figure 2. Contour graphs show the reflectivity (real index) and phase difference (imaginary index) of an example design with ns = 1.5, nf1 = 1.7 and nf2 = 1.4. (a) nf1 deposited on top of ns. (b) nf2 deposited on top of nf1. Both films are quarter-wave thick.

The limitation of using QWOT films for AR design is the selection of materials with correct refractive index. An easier method is to control the thickness of each film. This can be achieved by drawing the full contours circle for both films. The contour of the first film is plotted from the substrate index like usual. But the second film contour is plotted from the air. For example, a common substrate is SiO2 with ns = 1.48, Al2O3 a refractive index of nf1 = 1.77 similar, and MgF2 is nf2 = 1.38, as shown in Figure 3.

Figure 3. Contour graph shows the reflectivity of an example design with ns = 1.48, nf1 = 1.77 (red) and nf2 = 1.38 (green).

The interception points of the two lines can be solved for thicknesses with non-linear solver, such as fsolve. The number of answers in this example is two, as shown in Figure 4.

Figure 4. Contour graphs show the two possible answers for perfect antireflection.

#### 2.2.3 Asymmetrical resonance cavity design

A resonant cavity is a useful design for enhancing the optical properties of central cavity layer, which in this study will be PCM. A distributed Bragg reflector cavity consists of two reflecting layers placed on either side of the central layer. The two reflectors cause light to cycle through the central layer multiple times, which effectively reduced the required thickness of PCM. The mirror on each side is created from a unit cell (U) composed of materials with high (H) and (L) refractive index with quarter-wave optical thickness. The larger the difference, the better the enhancement. In this work, unit cells will be denoted as [H/2 L H/2], where 1/2 indicates a film with half the QWOT. As an example, if we use 1 unit cell on each side, and also have H as the central cavity layer, the structure can be written as:

.		 		   (16)

By combining the central H with the two adjacent H/2, we get

.			 		       (17)

The combination of two QWOT films with the same index creates half-wave optical thickness (HWOT) layer, which is equivalent to an absentee layer (loss less). The two adjacent Hs and the two Ls can be combined, with the final structure reduced to an equivalent of a single quarter-wave thick H layer

,						  (19)

H.					           (20)

For a multi-unit-cell design, the notation of Eq. (16) can be rewritten as [U]N C [U]M, where N is the number of unit cell on the substrate side, C is the central cavity layer (H in this example), and M is the number of unit cell on the incident side.

But when the central cavity layer is made from PCM or metal, their refractive index has a value in the imaginary term (extinction coefficients; k). This absorption leads to a loss of resonance. Figure 5 demonstrates the effect with symmetrical U3 on each side, nH = 2.23, nL = 1.46. For figure 5a a resonant can be created with central layer consisted of only the real part in the refractive index, nC = 3.15. But figure 5b with nC = 3.15 - i0.35, an AR design is impossible.

Figure 5. Contours of 3 unit-cells symmetrical cavity. Blue is the number of unit cells on the substrate side N, red is the number on the incident side M, and green is the central layer C. (a) The central layer is made from nC = 3.15. (b) The central layer has extinction coefficient, nC = 3.15 - i0.35, which moves the final nr away from na. Reprinted from [35].

To partially restore the AR condition, the number of unit cells of the incident side is reduced to 1, as shown in figure 6. This redesign adjusts the final nr closer to na.

Figure 6. Contour of asymmetrical cavity. With reduced number of unit cells on the incident side to M = 2 (red) the final nr is now closer to na. Reprinted from [35].

A resonant can be fully restored by adding a compensatory layer with zero extinction coefficient in the central layer, as shown in figure 7.

Figure 7. Contour of a restored resonant cavity. The compensator layer (yellow) can be made from dielectric with appropriate thickness. Also reprinted from [35].

#### 2.2.4 Derivation of transfer-matrix for resonant cavity structure

The optical response of the designed resonant cavity structure is calculated by the transfer matrix method (TMM), which is widely used for one dimensional multilayer thin film systems [43-45]. The device consists of a phase change Sb₂Se₃ cavity layer C embedded between two distributed Bragg reflector (DBR) sections with different numbers of unit cells on the incident side (M) and on the substrate side (N). Each DBR unit cell is composed of a low index layer L and two half thickness high index layers H/2 at the cell boundaries, so that the whole stack can be illustrated as figure 8 [43-45]. Here, the whole cavity structure is embedded between a semi-infinite incident medium (air) and a semi-infinite substrate. This configuration ensures that the cavity is always bounded by an H/2 layer on both sides, and asymmetry is introduced only by the different numbers of unit cells M and N.

Figure 8. A schematic of the resonant cavity structure.

For a monochromatic plane wave of free-space wavelength λ incident from air (index n0) at angle θ0, the electric field in layer j is written as a superposition of forward and backward waves:

, 				      (21)

with longitudinal wavevector:

, 				           (22)

where  is the complex refractive index and θj is the internal angle obtained from Snell’s law

. 				            (23)

Eq. (23) is applied successively to all layers because all interfaces are parallel. For each layer j, it is convenient to introduce the column vector of forward and backward amplitudes in layer j,

. 					      (24)

At the interface between layer j and j+1, continuity of the tangential components of electric and magnetic fields gives the Fresnel reflection and transmission coefficients. For TE polarization, these coefficients are:

, . 	        (25a)

For TM polarization, the Fresnel coefficients are:

, . 	        (25b)

Then the interface matrix relating to Ej and Ej+1 is:

, . 			      (26)

Propagation through a homogeneous layer j of thickness dj simply multiplies the forward and backward amplitudes by phase factors. In terms of Ej, we can write at the entrance (z = 0) and exit (z = dj) of the layer:

.

This is compactly expressed as:

,				     (27)

with the propagation matrix

, 			    (28)

Thus, every interface contributes one interface matrix Ij,j+1 and every physical layer contribute one propagation matrix Pj. The TMM solution is obtained by multiplying these matrices in the correct order.

According to the structure in figure 8, optical wave incident from air, then pass through M unit cells on the left DBR, the cavity layer C, and N unit cells on the right DBR, and finally reach the substrate. For TE polarization, the total system matrix M can be obtained by multiplying all interface and propagation matrices in the order of the physical stack as:

. 	(29)

Denoting the field amplitudes in air and substrate by E0 and EsubEsub, respectively,

. 			               (30)

Assuming no incoming wave from the substrate Esub-0(), Eq. (30) yields

. 		                 (31)

Dividing the second row of Eq. (31) by the first gives the reflection amplitude, and dividing the substrate amplitude by the incident amplitude gives the transmission amplitude:

, , 			          (32)

where Mij are the elements of MM. Eq. (32) is thus a direct algebraic consequence of Eq. (31), which results from inserting the system matrix (29) into the field relation (30). Finally, the power reflectance, transmittance, and absorbance are obtained from the amplitudes in Eq. (32). The reflectance is simply as:

, 				        (33)

while the transmittance must be corrected for the ratio of normal Poynting fluxes in substrate and incident medium,

, 			          (34)

where θsubθsub is given by Snell’s law in Eq. (23) and Re[…] denotes the real part. Conservation of energy then gives the absorbance:

, 			          (35)

which includes all absorption in the lossy layers such as Sb₂Se₃ and any non-radiative loss.

#### 2.2.5 Endurance metrics of resonant cavity based optical limiter

Endurance of the Sb₂Se₃ resonant cavity based optical limiter is characterized by how its optical response degrades with the number of amorphous–crystalline switching cycles Ncyc [14]. By inserting the complex refractive index of Sb₂Se₃ for empirical endurance modeling as Eq. (17) into the TMM framework of sub-section 2.2.4, then the transmittances of the resonant cavity based optical limiter at amorphous and crystalline states;  and  can be computed numerically. These transmittances will be important part of optical limiter endurance metric calculation. Here, the endurance metrics are composed of transmitting contrast [14], insertion loss [45], and failure cycle [46-47], all defined at a chosen operating wavelength λ0 and incident angle θ0. Since endurance drift in np(Ncyc) and kp(Ncyc) as mentioned above, therefore, endurance metrics for our structures can directly be written as a change of Ta(Ncyc) and Tc(Ncyc).

- Transmitting Contrast Degradation

The linear and normalized transmitting contrast between crystalline and amorphous states at cycle Ncyc is defined as:

, 			       (36a)

and

, 			         (36b)

where T0 = Tc(1) is initial transmittance at crystalline phase. Let ΔT0 = ΔT(1) be the initial transmitting contrast. Then the transmitting contrast degradation in relative and percentage form are written as:

, 					(37a)

and

. 			      (37b)

- Insertion loss

The insertion loss of the cavity at cycle Ncyc compares its transmittance to a reference state. Choosing the initial crystalline state as reference 46:

. 			     (38)

A growing ILdB(Ncyc) indicates increasing loss, typically driven by the linear growth of the imaginary index kp(Ncyc) and by detuning of the resonance due to drift of np(Ncyc).​

- Failure criterion and endurance lifetime

A failure cycle Nfail is defined when one or more endurance metrics cross specified limits, for example:

- Transmitting contrast degradation exceeds a maximum value: .

- Insertion loss exceeds the maximum value: .

The endurance lifetime of the optical limiters is then specified as the number of reliable switching cycles, typically taken as NfailNfailNfail-1, providing a quantitative link between microscopic drift in Sb₂Se₃ optical constants and macroscopic degradation of optical-limiting performance. In this study, our optical limiters should still maintain reliability when transmitting contrast degradation: Dpct and insertion loss: ILdB are not over Dpct,max = 20% and ILdB,max = 2 dB, respectively [46-48]. These criteria are aligned with normal requirements of photonic switching devices.

#### 3. Numerical results and discussions

3.1 Optical limiting performance of our designed samples

3.2 Numerical characterizations of optical limiters’ endurance

To examine the optimal designed optical limiter stability by using the endurance metrics mention in sub-section 2.2.3, we performed 2.5 – 3.0 million cycles for thermally induced phase transitions to two selected samples for two operating wavelengths such as 532 nm and 1,064 nm. In all cases, we assume that our structures are beginned with amorphous state and then thermally induced to crystalline state back and fourth until last cycle. Our calculations starts with the transmittances of our resonant cavity structures vs number of cycles, when Sb2Se3 is amorphous and crystalline phase. These tranmittances lead to obtain the transmitting constrast as definition in Eqs. (21). Both transmittances and transmitting contrasts are used to calculated the important two endurance metrics such as contrast degradation and insertion loss of our structures when they are applied by multi-million optical cycles. The endurance metrics will confirm us how our structures are good optical limiter.

3.2.1 Endurance testing of the resonant optical limiter for operating wavelength 532 nm

Endurance metrics for 532 nm-optical limiting: Nfail > 2.5 × 106 cycles, Drel = 20%, ILdB = 0.61 dB

The long-term reliability testing of the 532 nm-resonant optical limiter is illustrated in Figure 9. The device exhibits stable performance across millions of thermo-optical cycles, showing only a minor and controlled decline in endurance parameters.

The calculated transmittance in the amorphous and crystalline states, as shown in figure 9a, remains highly stable over more than five decades of cycling number, which confirms the good endurance of the proposed phase‑change device. In the amorphous phase, the transmittance Ta (red dashed-dotted line) is nearly constant at about 0.5 for low and intermediate cycle numbers and only begins to decrease slightly when the cycling number exceeds 106, whereas the crystalline‑state transmittance Tc (blue dashed-dotted line) stays around 0.24 and shows only a modest reduction in the high‑cycle regime; this behavior indicates that both the ON and OFF states preserve their optical levels with minimal drift during most of the cycling window.

The normalized transmitting contrast ΔT/T0, is illustrated as magenta dashed-dotted curve in figure 9b defined as the transmittance difference between the amorphous and crystalline states normalized to its initial value, is almost constant at approximately −0.145 from the first cycle up to around 105 – 106 cycles. A noticeable change appears only in the high‑cycle region, where ΔT/T0 gradually decreases toward about −0.18, revealing a moderate degradation of modulation depth that can be attributed to accumulated structural fatigue or slight index drift in the phase‑change layer and surrounding interfaces.

According to figure 9c, the transmitting contrast degradation Dpct, evaluated as the relative loss of transmitting contrast in percent, remains essentially negligible (well below 1%) for cycle numbers below 105, which demonstrates that the device can undergo a large number of switching events without significant penalty in contrast. Beyond this region, Dpct increases rapidly and reaches values above 20% when the cycling number approaches 107, indicating the onset of a failure regime in which repeated amorphous–crystalline transitions induce noticeable deterioration of the achievable transmission contrast.

Finally, the insertion loss is examined and represented as green dashed-dotted curve in figure 9d. Here, the insertion loss, expressed in decibels, is very close to 0 dB over a wide cycling range up to about 105 – 106 cycles, confirming that the device introduces almost no additional attenuation to the transmitted signal in its useful operating regime. When the number of cycles further increases toward 107, the insertion loss becomes more pronounced and drops to roughly −0.6 to −0.7 dB, which is consistent with the observed contrast degradation and suggests that cumulative material and interface changes start to reduce the overall throughput of the structure while still keeping the excess loss at a relatively low level.

| (a) | (b) |
| --- | --- |
| (c) | (d) |

#### Figure 9. Results of endurance testing for 532-nm-optical limiter sample consist of transmittances T of (a) the amorphous (red) and (b) crystalline phases, normalized to initial transmittance in crystalline phase T0, (c) transmitting contrast degradation, and (d) insertion loss as a function of the cycle number.

3.2.2 Endurance testing of the resonant optical limiter for operating wavelength 1,064 nm

Endurance metrics for 1,064 nm-optical limiting: Nfail ≈ 2 × 106 cycles, Drel = 20%, ILdB = 0.61 dB

Endurance testing of the 1064 nm-resonant optical limiter as shown in figure 10 demonstrates that the device maintains stable operation over multimillion thermo‑optical cycles, with gradual but manageable degradation in its key endurance metrics.

According to figure 10a, in the amorphous state, the transmittance Ta stays very close to unity from the first cycle up to about 105 - 106 cycles and only exhibits a slight decrease when the cycle number approaches 107, which means that the “ON” state of the switch remains highly transparent throughout most of the endurance window. In the crystalline state, the transmittance Tc is much lower (around 0.25–0.28) but also shows only a weak dependence on the cycling number until the high‑cycle regime, where a modest reduction is observed, confirming that the “OFF” state maintains a strong attenuation with minimal fatigue‑induced drift. Then, the normalized transmitting contrast as illustrated by magenta curve in figure 10b, defined as the relative difference in transmittance between the amorphous and crystalline states with respect to the initial contrast, remains almost constant over more than five decades of cycling number, which demonstrates the robustness of the optical modulation mechanism. A noticeable degradation of ΔT/T0 is observed only when the cycle number approaches the 106 - 107 range, where the contrast begins to decrease from approximately − 0.36 to about − 0.45, suggesting the onset of fatigue‑induced structural or compositional changes in the phase‑change layer.

After that, we consider the endurance metrics for our devices at operating wavelength 1,064 nm. First, the transmitting contrast degradation: Dpct, which is represented by cyan curve in figure 10c, remains negligible (<1%) up to around 105 cycles and then increases steeply beyond 106 cycles, reaching values on the order of 20–25%, which quantitatively confirms that the device maintains nearly stable contrast over most of its cycling lifetime before a rapid degradation regime sets in. Next, the insertion loss: ILdB, as shown in figure 10d, stays very close to 0 dB for cycle numbers below approximately 105, indicating that the device introduces almost no additional attenuation to the transmitted signal in its operational window. When the number of cycles exceeds roughly 106, the insertion loss increases rapidly down to about − 0.6 to − 0.7 dB, reflecting the cumulative effect of material fatigue and interface degradation on the overall transmission, yet remaining relatively low compared with typical optical interconnect tolerances as mentioned in sub-section 2.2.3. From both endurance metrics, we found that the failure cycle: Nfail is around at cycle number 2 × 106 because the contrast degradation becoming over 20%. So that, we can recommend that, at wavelength 1,064 nm, our optical limiter should not be used over 2 × 106 cycles of optical switching.

| (a) | (b) |
| --- | --- |
| (c) | (d) |

#### Figure 10. Results of endurance testing for 1,064-nm-optical limiter sample consist of transmittances T of (a) the amorphous (red) and (b) crystalline phases, normalized to initial transmittance in crystalline phase T0, (c) transmitting contrast degradation, and (d) insertion loss as a function of the cycle number.

#### 4. Fabrication guidance of resonant optical limiter

The resonant cavity shown in figure 8 consists of a thin Sb₂Se₃ phase change layer C embedded between two DBR sections, each formed by repeated (H/2∣L∣H/2) unit cells with equal or different numbers of periods M and N. For practical implementation on a chip or glass substrate, the device can be fabricated using standard thin film deposition and lithographic processes compatible with integrated photonics [16, 37]. The fabrication process is composed of below steps:

Step 1 – Substrate preparation

An optically flat substrate such as fused silica or Si wafer with thermally grown SiO₂ is cleaned using solvent baths (acetone, isopropanol, de‑ionized water), dried with nitrogen, and treated by oxygen plasma or UV‑ozone to remove organic residues and improve adhesion for subsequent films.

Step 2 – Deposition of bottom DBR (N unit cells)

The bottom distributed Bragg reflector is deposited by sputtering, PECVD, or e‑beam evaporation of a high‑index material H e.g. Si₃N₄ and a low‑index material L e.g. SiO₂. Each unit cell (H/2∣L∣H/2) is formed by sequentially depositing a half‑thickness H layer, a full L layer, and another H/2 layer with optical thicknesses close to the designed quarter‑wave values; this unit cell is repeated N times to obtain a high‑reflectivity bottom DBR at the target wavelength.

Step 3 – Deposition of Sb₂Se₃ cavity layer

On top of the bottom DBR, an amorphous Sb₂Se₃ layer of designed thickness (typically 20–100 nm) is deposited by RF sputtering from a stoichiometric target or by thermal evaporation. The substrate temperature is kept below the crystallization temperature to preserve the amorphous phase, and an optional few‑nanometer SiO₂ capping layer can be added in situ to protect Sb₂Se₃ and suppress interdiffusion, which improves long‑term stability and cycling endurance.

Step 4 – Deposition of top DBR (M unit cells)

The top DBR is then grown on the Sb₂Se₃ (or its cap) using the same H and L materials as the bottom DBR. Starting from an H/2 layer directly above the cavity, the (H/2∣L∣H/2) sequence is repeated M times, creating a DBR with a different number of unit cells compared with the bottom reflector and thus producing the required asymmetry while maintaining matching boundary layers at the cavity interfaces. Thickness control for each layer again follows the quarter‑wave design to ensure that the stop band and cavity resonance match the optical design.

Step 5 – Device patterning and optional heater integration

If discrete devices are needed, the continuous multilayer film is patterned into mesas using photolithography and reactive‑ion etching, so each mesa contains one DBR/Sb₂Se₃/DBR cavity of defined lateral size. For electro‑thermal operation, thin‑film metal heaters or electrodes (e.g. TiN, Cr/Au) are deposited and patterned adjacent to, or partly overlapping, the cavity region to allow controlled Joule heating of Sb₂Se₃ during programming pulses.

​Step 6 – Post‑processing and characterization

A mild post‑deposition annealing step may be applied to relieve stress and stabilize interfaces while keeping Sb₂Se₃ in the desired initial phase. The final structure is characterized by spectroscopic ellipsometry and reflectance/transmittance measurements to confirm layer thicknesses, refractive indices, and resonance position, followed by cycling and optical‑limiting experiments to verify transmission contrast, switching threshold, and endurance of the fabricated resonant optical limiter.​

#### 5. Conclusions

#### References

[1] M. Wuttig, H. Bhaskaran, and T. Taubner, “Phase-change materials for non-volatile photonic applications,” Nat. Photonics 11(8), 465–476 (2017).

[2] K. Matuszek, M. Kar, J. M. Pringle, and D. R. MacFarlane, “Phase change materials for renewable energy storage at intermediate temperatures,” Chem. Rev. 123(1), 491–514 (2023).

[3] R. Matos and N. Pala, “A review of phase-change materials and their potential for reconfigurable intelligent surfaces,” Micromachines 14(6), 1259 (2023).

[4] A. Sarangan, J. Duran, V. Vasilyev, N. Limberopoulos, I. Vitebskiy, and I. Anisimov, “Broadband reflective optical limiter using GST phase change material,” IEEE Photonics J. 10(2), 1–9 (2018).

[5] R. Heenkenda, K. Hirakawa, and A. Sarangan, “Tunable optical filter using phase change materials for smart IR night vision applications,” Opt. Express 29(21), 33795–33803 (2021).

[6] D. de Ceglia, M. Grande, A. Vincenti, C. Baratto and C. de Angelis, "Tunable filters for visible light based on resonant VO2 planar thin films," 2020 22nd International Conference on Transparent Optical Networks (ICTON), Bari, Italy, 2020, pp. 1-4.

[7] H. Kocer et al., “Intensity tunable infrared broadband absorbers based on VO2 phase transition using planar layered thin films,” Sci. Rep. 5(1), 13384 (2015).

[8] X. Tian and Z.-Y. Li, “An optically-triggered switchable mid-infrared perfect absorber based on phase-change material of vanadium dioxide,” Plasmonics 13(4), 1393–1402 (2018).

[9] E. Strelcov, Y. Lilach, and A. Kolmakov, “Gas sensor based on metal−insulator transition in VO2 nanowire thermistor,” Nano Lett. 9(6), 2322–2326 (2009).

[10] R. Kononchuk, S. Suwunnarat, M. S. Hilario, A. E. Baros, B. W. Hoff, V. Vasilyev, I. Vitebskiy, T. Kottos, and A. A. Chabanov, “A free-space mm-wave photonic limiter,” 2022 Conference on Lasers and Electro-Optics (CLEO), San Jose, CA, USA, 2022, pp. 1-2.

[11] M. G. Wood, A. McKay, T. J. Morin, D. K. Serkland, T. S. Luk, S. L. Wolfley, L. Gastian, J. P. Mudrick, B. Jasperson, and H. T. Johnson, “Optically-triggered optical limiters for short-wavelength infrared sensor protection,” 2021 Conference on Lasers and Electro-Optics (CLEO), San Jose, CA, USA, 2021, pp. 1-2.

[12] C. Wan, Z. Zhang, J. Salman, J. King, Y. Xiao, Z. Yu, A. Shahsafi, R. Wambold, S. Ramanathan, and M. A. Kats, “Ultrathin broadband reflective optical limiter,” Laser Photonics Rev. 15(6), 2100001 (2021).

[13] P. Xu, J. Zheng, J. K. Doylend, and A. Majumdar, “Low-loss and broadband nonvolatile phase-change directional coupler switches,” ACS Photonics 6(2), 553–557 (2019).

[14] D. Lawson, S. Blundell, M. Ebert, O. L. Muskens, and I. Zeimpekis, “Optical switching beyond a million cycles of low-loss phase change material Sb2Se3,” Opt. Mater. Express, 14(1), 22–38 (2024).

[15] C. Wan, E. H. Horak, J. King, J. Salman, Z. Zhang, Y. Zhou, P. Roney, B. Gundlach, S. Ramanathan, R. H. Goldsmith, and M. A. Kats, “Limiting optical diodes enabled by the phase transition of vanadium dioxide,” ACS Photonics 5(7), 2688–2692 (2018).

*[16] M. Delaney, I. Zeimpekis, D. Lawson, D. W. Hewak, and O. L. Muskens, “A new family of ultralow loss reversible phase-change materials for photonic integrated circuits: Sb2S3 and Sb2Se3,” Adv. Funct. Mater. 30(36), 2002447 (2020).

[17] Y. Zhang, J. B. Chou, J. Li, H. Li, Q. Du, A. Yadav, S. Zhou, M. Y. Shalaginov, Z. Fang, H. Zhong, C. Roberts, P. Robinson, B. Bohlin, C. Rios, H. Lin, M. Kang, T. Gu, J. Warner, V. Liberman, K. Richardson, and J. Hu, “Broadband transparent optical phase change materials for high-performance nonvolatile photonics,” Nat. Commun. 10(1), 4279 (2019).

[18] Z. Gong, F. Yang, L. Wang, R. Chen, J. Wu, C. P. Grigoropoulos, and J. Yao, “Phase change materials in photonic devices,” J. App. Phys. 129(3), 030902 (2021).

[19] M. E. A. Warwick and R. Binions, “Advances in thermochromic vanadium dioxide films,” J. Mater. Chem. A 2(10), 3275–3292 (2014).

[20] P. Guo, Z. Biegler, T. Back, and A. Sarangan, “Vanadium dioxide phase change thin films produced by thermal oxidation of metallic vanadium,” Thin Solid Films 707, 138117 (2020).

[21] Y. Cui, Y. Ke, C. Liu, Z. Chen, N. Wang, L. Zhang, Y. Zhou, S. Wang, Y. Gao, and Y. Long, “Thermochromic VO2 for energy-efficient smart windows,” Joule 2(9), 1707–1746 (2018).

[22] N. Murillo-Quirós, V. Vega-Garita, A. Carmona-Calvo, E. A. Rojas-González, R. Starbird-Perez, and E. Avendaño-Soto, “Toward thermochromic VO2 nanoparticles polymer films based smart windows designed for tropical climates,” Polymers 14(19), 4250 (2022).

[23] C. Chen, W. Li, Y. Zhou, C. Chen, M. Luo, X. Liu, K. Zeng, B. Yang, C. Zhang, J. Han, and J. Tang, “Optical properties of amorphous and polycrystalline Sb2Se3 thin films prepared by thermal evaporation,” Appl. Phys. Lett. 107, 043905 (2015).

[24] X. Chen, J. Lin, and K. Wang, “A review of integrated photonic devices using Sb2Se3,” Adv. Phys. Res. 4(1), 2400080 (2025).

[25] K. Aryana, H. J. Kim, Md. R. Islam, N. Hong, C. Popescu, S. Makarem, T. Gu, J. Hu, and P. E. Hopkins, “Optical and thermal properties of Ge2Sb2Te5, Sb2Se3, and Sb2S3 for reconfigurable photonic devices [Invited],” Opt. Mater. Express, 13(11), 3277–3286 (2023).

[26] J. Faneca, I. Zeimpekis, S. T. Ilie, T. D. Bucio, K. Grabska, D. W. Hewak, and F. Y. Gardes, “Towards low loss non-volatile phase change materials in mid index waveguides,” Neuromorph. Comput. Eng. 1(1), 014004 (2021).

[27] S. Blundell, T. W. Radford, I. A. Ajia, D. Lawson, X. Yan, M. Banakar, D. J. Thomson, I. Zeimpekis, and O. L. Muskens, “Ultracompact programmable silicon photonics using layers of low-loss phase-change material Sb2Se3 of increasing thickness,” ACS Photonics 12(3), 1382–1391 (2025).

[28] W. Jia, R. Menon, and B. Sensale-Rodriguez, “Unique prospects of phase change material Sb2Se3 for ultra-compact reconfigurable nanophotonic devices,” Opt. Mater. Express, 11(9), 3007–3014 (2021).

[29] M. Gandolfi, A. Tognazzi, B. Li, G. Ambrosio, R. Camacho Morales, C. Baratto D. De Ceglia, A. C. Cino D. N. Neshev, and C. De Angelis, “Optical limiting thin multilayer films based on phase transition in VO2,” 2022 Sixteenth International Congress on Artificial Materials for Novel Wave Phenomena (Metamaterials), Siena, Italy, 2022, pp. 148-150.

[30] C. Baratto, M. Gandolfi, A. Tognazzi, P. Franceschini, G. Ambrosio, B. Li, R. Camacho Morales, D. de Ceglia, A. C. Cino D. N. Neshev, and C. De Angelis, “Optical limiting sensor based on multilayer optimization of Ag/VO2 phase change material,” IEEE Sens. Lett. 7(9), 1–3 (2023).

[31] A. Tognazzi, M. Gandolfi, B. Li, G. Ambrosio, P. Franceschini, R. Camacho-Morales, A. C. Cino, C. Baratto, D. de Ceglia, D. Neshev, and C. De Angelis, “Opto-thermal dynamics of thin-film optical limiters based on the VO2 phase transition,” Opt. Mater. Express 13(1), 41–52 (2023).

[32] A. Sarangan, “Design of resonant cavity thin film structures with complex active layers,” J. Opt. Soc. Am. B, 37(11), 3461–3468 (2020).

[33] Y. Huang, C. Lee, M. Rath, V. Ferrari, H. Yu, T. J. Woehl, J. H. Ni, I. Takeuchi, and C. Ríos, “Tunable structural transmissive color in fano-resonant optical coatings employing phase-change materials,” Mater. Today Adv. 18, 100364 (2023).

[34] A. Sarangan, Optical Thin Film Design, 1st Edition ed. Boca Raton: CRC Press, 2020.

[35] C. Padungatthakij, S. Wicharn, and P. Buranasiri, “Asymmetrical resonant cavity thin film devices designed for vanadium dioxide applications,” Proc. of SPIE 13663, 1366304 (2025).

[36] Md. S. Alam, R. Laing, Z. Bolatbek, R. H., R. Gnawali, T. E. Payne, A. Sarangan, J. R. Hendrickson, and I. Agha, “Fast cycling speed with multimillion cycling endurance of ultra-low loss phase change material (Sb2Se3) by engineered laser pulse irradiation,” Adv. Funct. Mater. 34(14), 2310306 (2024).

[37] K. Aryana, H. J. Kim, Md. R. Islam, N. Hong, C. Popescu, S. Makarem, T. Gu, J. Hu, and P. E. Hopskin, “Optical and thermal properties of Ge2Sb2Te5, Sb2Se3, and Sb2S3 for reconfigurable photonic devices [Invited],” Opt. Mater. Express 13(11), 3277–3286 (2023).

[38] M. Delaney, I. Zeimpekis, H. Du, X. Yan, M. Banakar, D. J. Thomson, D. W. Hewak, and O. L. Muskens, “Nonvolatile programmable silicon photonics using an ultralow-loss Sb2Se3 phase change material,” Sci. Adv. 7(25), eabg3500 (2021).

[39] K. Murali, L. Thekkekara, Md. A. Rahman, S. Sen, V. Shvedov, Y. Izdebskaya, C. Zou, S. A. Tawfik, I. Shadrivov, S. Sriram, and M. Bhaskaran, “Tunability of Sb2Se3 phase change material for multi-domain optoelectronics,” Appl. Mater. Today 40, 102338 (2024).

[40] Y. Zhang, C. Ríos, M. Y. Shalaginov, M. Li, A. Majumdar, T. Gu, and J, Hu, “Myths and truths about optical phase change materials: A perspective,” Appl. Phys. Lett. 118, 210501 (2021).

[41] L. Martin-Monier, C. C. Popescu, L. Ranno, B. Mills, S. Geiger, D. Callahan, M. Moebius, and J. Hu, “Endurance of chalcogenide optical phase change materials: a review,” Opt. Mater. Express 12(6), 2145–2167 (2022).

[42] S. Kim, G. W. Burr, W. Kim, and S. Nam, “Phase-change memory cycling endurance,” MRS Bull. 44(9), 710 – 714 (2019).

[43] P. Yeh, Optical Waves in Layered Media (Wiley, New York, 1988), Chap. 6.

[44] L. N. Acquaroli, “Matrix method for thin film optics,” arXiv preprint arXiv: 1809.07708v1.

[45] B. S. Danis and E. Zayim, “TMMax: High-performance modeling of multilayer

thin-film structures using transfer matrix method with JAX,” J. Open Source Softw. 10(114), 9088 (2025).

[46] R. Paschotta, article on insertion loss in the Encyclopedia of Laser Physics and Technology, 1. edition October 2008, Wiley-VCH, ISBN 978-3-527-40828-3.

[47] L. Tian, Y. Kuang, Z. Fan, and Z. Li, “Low insertion loss silicon-based spatial light modulator with high reflective materials outside Fabry–Perot cavity,” Chin. Phys. B 28(10), 104209 (2019).

[48] Z. Fang, R. Chen, J. Zheng, A. I. Khan, K. M. Neilson, S. J. Geiger, D. M. Callahan, M. G. Moebius, A. Saxena, M. E. Chen, C. Rios, J. Hu, E. Pop, and A. Majumdar, “Ultra-low-energy programmable non-volatile silicon photonics based on phase-change materials with graphene heaters,” Nat. Nanotechnol. 17, 842–848 (2022).

#### Appendix 1: Derivation of Endurance Model for Complex Refractive Index of Sb₂Se₃

- This appendix presents a simple derivation of the endurance model used for the real and imaginary parts of the complex refractive index of Sb₂Se₃ as a function of cycle number Ncyc as Eq. (2). The goal is to obtain compact expressions that can be directly used in the transfer-matrix simulations of the asymmetric cavity, while still being physically motivated by relaxation and damage processes observed in phase-change materials (PCMs) [1, 3, 9-11].

- X.1 Physical Picture and State Variable

- During repeated amorphous–crystalline switching, the microscopic structure of Sb₂Se₃ is not perfectly reversible. Processes such as structural relaxation, vacancy ordering, defect accumulation, and interface degradation gradually modify the optical response [9, 11]. To describe this in a simple way, introduce an internal state variable Xp(Ncyc) Xp(N)for each phase: p denotes amorphous (a) and crystalline (c). This variable is not specified microscopically; it represents the average structural state that affects the optical constants.

- We then assume:

- After many cycles, the material approaches a saturated equilibrium state Xp,∞ (relaxed or aged state).

- The real part of the refractive index np(Ncyc) is a monotonic function of this structural state and can be approximated as directly proportional to it:  [9-10].

- The imaginary part kp(Ncyc)kp(N) mainly reflects cumulative damage (defects, voids, roughness) and grows approximately linearly with the amount of damage [9-10].​

- Based on these assumptions, we derive separate models for np(Ncyc) and kp(Ncyc).

- X.2 Exponential Drift of Real Refractive Index

- For the structural state Xp(Ncyc), we postulate a first-order relaxation law with respect to cycle number Ncyc:

- , 			       (X.1)

- where αp > 0 is an effective relaxation (drift) rate per cycle for phase p [9].

- This equation says:

- If Xp(Ncyc)Xp(N) is larger than its equilibrium value Xp,∞, it decreases; if smaller, it increases.

- The rate of change is proportional to the deviation Xp-Xp,∞.

- Such first-order equations are standard in many PCM models for structural relaxation and resistance drift, where the property approaches a saturated value exponentially with time or accumulated stress [9, 11].

- Now, rewriting Eq. (X.1):

- . 			      (X.2)

- This is a linear first-order ordinary differential equation. Its homogeneous part is

- , 				          (X.3)

- with solution:

- , 				(X.4)

- where C is an integration constant. A particular solution to Eq. (X.2) can be chosen as constant:

- . 				          (X.5)

- Substituting Eq. (X.5) into Eq. (X.2):

- .

- So, Eq. (X.5) satisfies the rate equation. Then the general solution can be written as the sum of homogeneous and particular solutions as:

- . 		 (X.6)

- Let the initial state at Ncyc = 0 be Xp(0) = Xp,0 and using Eq. (X.6):

- . 			        (X.7)

- Therefore,

- . 				        (X.8)

- Substituting C back into Eq. (X.6):

- . 			  (X.9)

- Rearranging Eq. (X.9),

- . 			(X.10)

- We now assume the real refractive index in phase p follows this relaxation law:

- . 		     (X.11)

- Then Eq. (X.10) becomes

- . 			         (X.12)

- This is the endurance model used in the main text for the real part of the refractive index. The initial refractive index: np,0 is na,0 for amorphous phase and is nc,0 for crystalline phase. The asymptotic index: np,∞ is na,∞ = na,0 - nc,0 when amorphous phase transiting to crystalline phase and is nc,∞ = nc,0 - na,0 when crystalline phase switching back to amorphous phase. The drift rate αp controls how quickly the index approaches its saturated value. A larger αp gives a faster change in the first cycles, leading to quicker degradation of resonance condition and contrast. A smaller αp means slower drift and better long-term stability [3, 10].​ Exponential approach is consistent with many relaxation processes in PCMs and provides a simple, saturating law that fits property evolution under annealing or cycling, as reported for optical and electrical parameters [1, 9-11].

- X.3 Linear Growth of Imaginary Refractive Index

- While the real part reflects long-range structural ordering, the imaginary part kp is mainly associated with material absorption and scattering. Under repeated cycling, mechanisms such as defect accumulation, void formation, interface roughness, and micro-cracks can gradually increase optical loss [3, 9-10]. Empirically, studies on optical PCM endurance often show that insertion loss or extinction coefficient increases approximately linearly with cycle number in the early-to-intermediate lifetime regime.

- There are two convenient but equivalent ways to write such linear growth: an absolute linear model and a relative (percentage) linear model. Assume that the increment of loss per cycle is approximately constant. In discrete form, this can be written as:

- , 				  (X.13)

- where γpγp is the absolute increase in kp per cycle. Iterating Eq. (X.13) from Ncyc = 0, 1, 2, ….., Ncyc, then, we get general form of the absolute linear model as:

- . 			            (X.14)

- Parameter γp has units of imaginary index per cycle and measures the absolute damage rate. If γp is small and kp,0 is very low (as for Sb₂Se₃ in the near-IR), then even after many cycles the loss remains small, consistent with high-endurance, low-loss behavior [1, 3].​ If γp is larger, the cavity becomes more lossy, reducing Q-factor, increasing insertion loss, and lowering switching contrast.

- Sometimes it is more intuitive to think in terms of relative change: the loss increases by a fixed percentage per cycle. Suppose that after Ncyc cycles, the total increase in loss is a fraction βpNcyc of the initial loss kp,0. Then this gives the relative linear model:

- ,

- , 			              (X.15)

- where βp is dimensionless (relative change per cycle) and relates with γp = βpkp,0. For modeling extinction coefficient kp degrading, both models in Eq. (14) and Eq. (15) are valid depending on whether the absolute or relative form is used. Eq. (X.15) with γp is more convenient. Meanwhile, Eq. (X.17) with βp is easier to interpret or fit.

- For low loss Sb₂Se₃ with very small kp,0, such doubling can still be acceptable in absolute terms; this aligns with reports of multi-million cycle optical switching with only modest degradation [1, 3-4].  The linear dependence in Ncyc is a first order approximation valid in the regime where damage accumulates gradually and before abrupt failure; more complex behaviors (e.g. nonlinear growth or saturation) can be introduced if detailed experimental data require it [3, 10].